Retarding thermal degradation in hybrid perovskites by ionic liquid additives

Rui Xia,a,b,c Zhaofu Fei,a Nikita Drigo,b Valentin I. E. Queloz,b Giulia Grancini,b Felix D. Bobbink,a Zhangjun Huang,a Xiaodong Fang,c Cristina Roldán-Carmona,b,* Mohammad Khaja Nazeeruddin,b,* Paul J. Dysona,*

a Dr. Rui Xia, Prof. Zhaofu Fei, Paul J. Dyson, Dr. Félix D. Bobbink, Zhangjun Huang.

Institut des Sciences et Ingénierie Chimiques, Ecole Polytechnique Fédérale de Lausanne (EPFL), CH-1015 Lausanne, Switzerland.

E-mail: paul.dyson@epfl.ch

b Dr. Rui Xia, Giulia Grancini, Valentin I. E. Queloz, Nikita Drigo, Cristina Roldán-Carmona, Prof. Mohammad Khaja Nazeeruddin.

Group for Molecular Engineering of Functional Materials Institute of Chemical Sciences and Engineering École Polytechnique Fédérale de Lausanne (EPFL), CH-1951 Sion, Switzerland.

E-mail: Cristina.roldancarmona@epfl.ch; mdkhaja.nazeeruddin@epfl.ch

c Dr. Rui Xia, Prof. Xiaodong Fang

Anhui Provincial Key Laboratory of Photonic Devices and Materials, Anhui Institute of Optics and Fine Mechanics, Chinese Academy of Sciences, Hefei 230031, China.

Abstract

Recent years have witnessed considerable progress in the development of solar cells based on lead halide perovskite materials. However, their intrinsic instability remains a limitation. In this context, we investigated the interplay between the thermal degradation and the hydrophobicity of perovskite materials. To this end, the 1-(4-ethenylbenzyl)-3-(tridecafluorooctyl)-imidazolium iodide (ETI) salt was employed as an additive in hybrid perovskites, endowing the photoactive materials with high thermal stability and hydrophobicity. The ETI dopant inhibits methylammonium (MA) permeation in methylammonium lead triiodide (MAPbI3) occurring due to intrinsic thermal degradation, by inhibiting out-diffusion of the MA+ cation, preserving the pristine material and preventing decomposition. With this simple approach, high efficiency solar cells based on the unstable MAPbI3 perovskite are markedly stabilized under maximum power point tracking (MPPT), leading to greater than twice the preserved efficiency after 700 hours of continuous light illumination and heating (60 ºC). These results suggest a strategy to tackle the intrinsic thermal decomposition of MAI, an essential component in all state-of-the art perovskite compositions.

Keywords: perovskite, solar cell, stability, ionic liquid, imidazolium salt, dopant.

Introduction

Perovskite technologies, with methylammonium lead triiodide (MAPbI3) perovskite as the leading light-harvesting material, have emerged as the unique candidates to supersede the efficiencies of current solar technologies while ensuring low costs. The current record (certified) power conversion efficiency (PCE) for a perovskite solar cell (PSC) is 22.7% [1]. Such a high PCE can be attributed to the high absorption coefficient, large charge carrier diffusion length, suitable bandgap and low trap density of the perovskite material [2-5]. Perovskites can be easily processed through simple fabrication techniques, leading to a polycrystalline film in which the morphology, grain size and thickness determine device performance [6-9]. Exceptional versatility, comprising numerous processing methodologies and device architectures are available, opening the way for a variety of applications. Nevertheless, the long-term stability of perovskite materials is still a major concern and represents a huge bottleneck to large-scale commercialization [10-12].

MAPbI3 and its derivatives decompose to their initial constituents in the presence of water, oxygen and/or UV-light [13, 14]. Although water, oxygen and UV-light can be partially avoided, additional thermally activated decomposition pathways are a more fundamental and unavoidable problem [15, 16]. In particular, temperature induced decomposition favors the out-diffusion of the cation in the form of volatile derivatives (CH3NH2 and HI among others), leading to a PbI2 enriched perovskite with a reduced performance [17, 18]. To overcome this issue, several strategies have been proposed including the use of small cross-link agents [19], more stable low dimensional perovskites [20, 21], or inorganic interlayers [22, 23]. However, the enhanced stabilities are only achieved at the expense of device efficiency and increased processing costs. In this respect, the simplest fabrication approach to meet low-cost and high quality crystallinity is the single-step spin-coating deposition [24, 25]. By including dopants, the thermodynamics and growth kinetics of the perovskite films can be modulated [26-28], adjusting the crystallinity and hydrophobicity of the layer. For example, the incorporation of specific small molecules such as ionic liquids (ILs) can retard crystal growth, modulate the crystal orientation and suppress surface defects [29-31]. In addition, ILs have other conducive properties including good conductivity, low vapor pressure and high thermal stability [31-33], that can be beneficial to the pristine material.

In this work, ETI, an imidazolium-based IL with a bulky, hydrophobic polyfluorinated substituent, was employed as an additive to stabilize MAPbI3, the most unstable state-of-the-art perovskite material. Our results suggest that the incorporation of ETI, even in very small quantities, considerably modifies the properties of the perovskite film as it: i) facilitates the complete conversion of precursor salts, ii) suppresses thermal decomposition pathway, and iii) provides outstanding hydrophobicity within the active material. By using this simple doping approach with ETI, high-efficiency solar cells with PCE = 19.12 % have been prepared, which retain 80 % of their initial efficiency after 700 h of continuous light illumination at 60 ºC, measured at MMPT, as well as under dark, humid conditions (40% moisture in air, 25 ºC). Our results demonstrate an easy and effective way to retard degradation by directly targeting the hybrid perovskite material, opening the path for exploring hydrophobic additives as a route to overcome thermal and water-based degradation.

Figure 1a shows a schematic diagram of the device configuration employing ETI as large hydrophobic dopant. The cell architecture contains a compact TiO2 layer of ~20 nm (c-TiO2) and a mesoporous TiO2 layer of ca. 200 nm as the electron transport material (mp-TiO2), into which MAPbI3 is infiltrated, forming an additional capping layer (ca. 300 nm). A thin film of Spiro-OMeTAD (ca. 200 nm) is then employed as the hole transporting material, finalizing the structure with ca. 80 nm of gold. A cross-sectional scanning electron microscopy (SEM) image of a typical device is presented in Figure 1b. We studied the influence of ETI on the perovskite material by incorporating different molar contents in the film precursor solutions (aETI, from 1 to 4 %), leading to MAPbI3: ETI blends (see XPS analysis in Figure S1). Note that due to the large spatial volume of the ETI IL, higher amounts (aETI > 4 %) of the dopant considerably affects film formation, producing non-homogeneous layers with poor film coverage and efficiency (Figure S2). In contrast, aETI ≤ 4 % preserves the optical properties of the films, as shown in the Uv-Vis absorption and photoluminescence (PL) spectra in Figure 1c, maintaining a high absorption coefficient and a constant bandgap close to 1.5 eV (Figure S3). Similarly, the time resolved photoluminescence (TRPL) decays suggest the absence of any impact into the charge carrier dynamics, showing identical carrier lifetimes of ~17 ns in all samples (Figure S4 and Table S1).

The influence of the ETI dopant on crystal growth was also investigated by X-ray diffraction (XRD). Figure 1d shows the diffraction patterns of perovskite films containing aETI ≤ 4%, including MAPbI3 as reference. A negligible impact on the crystal structure is detected, since MAPbI3 retains its tetragonal phase without the appearance of any additional peaks. This demonstrates the absence of any secondary crystalline structure involving the large organic cation [34]. There is, however, a low intensity diffraction peak at 12.7º in all samples, corresponding to unreacted PbI2. Similar observations has been reported to result from the high temperature annealing process (100 ºC), which induces MAI evaporation and the formation of residual PbI2 [35, 36]. Interestingly, the PbI2 signal is reduced as the ETI content increases (Figure 1e), suggesting enhanced perovskite conversion or an enhanced resistance to thermal treatment.

The morphology of the layers was also analyzed by SEM. Similar grain sizes and textures were observed for all samples, although some larger crystals were present in the films containing 1% ETI (Figure 1f). Small grain agglomerations, probably related with PbI2 formation as suggested by the XRD analysis, were also observed in all cases, which became less apparent as the ETI content increases (Figure S2). There is, however, a considerable number of pinholes at higher ETI concentrations, which reduces the compactness of the layers and negatively impacts on photovoltaic performance.

The current density-voltage (J-V) curves and photovoltaic parameters of the PSCs doped with ETI are provided in Figure 2a and Table S2, respectively. The devices employing MAPbI3 as the photoactive material exhibit an average PCE of 17.97% and a champion cell of 18.40% (Jsc=21.96 mA/cm2, Voc=1.07 V, FF=0.783), leading to a hysteresis factor (h) in the J-V curve close to 6% [37]. Similar behavior is also observed when ETI is incorporated into the system, with very high values of Voc, Jsc and FF observed when aETI < 4%. Interestingly, 1% ETI doping results in a markedly improved performance, boosting the efficiency to an average value of 18.57% and a champion cell of 19.12% (Jsc=22.37 mA/cm2, Voc=1.09 V, FF=0.784, h = 5%). Compared with the pristine cells, the current density is considerably augmented to values averaging over 22 mA/cm2. This enhancement may result from the increased levels of perovskite conversion based on the amount of residual PbI2 observed in the XRD analysis [38-40]. This is also supported by the external quantum efficiency (EQE) shown in Figure. 2b as increased photocurrent is detected for the 1% ETI doped device (J integrated for 0, 1, 2, and 4% ETI content are 21.64, 21.97, 21.53, and 20.88 mA/cm2 respectively, in agreement with the J-V parameters). Notably, a higher concentration of ETI does not have a beneficial effect, and the device performance decreases to values below 17%, mostly due to a significant drop in Voc. We relate the lower voltage to the increased number of pinholes previously observed in the SEM images, which may increase charge recombination and deteriorate device performance. A statistical analysis of the main photovoltaic parameters obtained from 15 samples in each group is presented in Figure 2c (see also Table S2). The hysteresis analysis of the different samples is also shown in Figure S5.

The device stability was also evaluated under light soaking conditions at MPPT. Figure 3b presents the stability curves comparing the devices containing MAPbI3 and the best performing ETI: MAPbI3 blend, i.e. the 1% ETI doped material. The unsealed devices, measured in an argon atmosphere and ca. 60 ºC under constant 100 mW/cm2 illumination, demonstrate a strong influence of the ETI IL in the stabilization of the perovskite system, preserving ca. 83% of the initial efficiency after 700 hours of continuous light illumination. In contrast, the cells based on MAPbI3 retain only 49% of the initial efficiency, in keeping with other reports [41]. We note here that MAPbI3 is a fragile material and rapidly undergoes thermal degradation at the temperature of the stability tests, resulting in a lower performance. A detailed inspection of the time evolution of the Jsc, Voc and FF values under MMPT is presented in Figure S6. Notably, despite all parameters deteriorating similarly in both systems, Jsc and Voc are greatly preserved in the ETI-doped system, which seems to be responsible for the improved stability. Along with the thermal effect, the stability was also evaluated in ambient air using non-encapsulated cells kept in a dark, humid environment. Similar results were obtained after aging the samples in 40 ± 5% humidity at room temperature. Under these conditions, the device with 1% ILs retains 80% of the initial PCE whereas the pristine cell retains only 59% (Figure 3b), confirming an improved resistivity against moisture (the variation in the Jsc, Voc, and FF trends are shown in Figure S6).

To further analyze these observations, the interplay between the ETI content and the thermal degradation in the films was investigated. We intentionally performed the analysis under an argon atmosphere and in the dark to determine the key degradation parameter induced by temperature, avoiding the effect of moisture, light and oxygen. Under these conditions a striking difference between samples appears at higher temperatures, denoting a difference in their resistance to decomposition. Figure 3c shows the XRD evolution for three different ETI:MAPbI3 blends (aETI ≤ 4 %), as well as the pristine material, after 720 hours of continuous thermal annealing at 60 ºC. Because degradation of the films can be correlated to the formation of PbI2, the analysis was focused in the region 2θ = 5-20º. Note that for the pristine MAPbI3, a diffraction peak corresponding to PbI2 (12.7°) increases considerably with time, suggesting continuous decomposition to the initial precursors under uninterrupted heat treatment. In contrast, ETI containing samples clearly preserve their initial features, demonstrating enhanced thermal stability at even 1% ETI. Such stabilization improves as the ETI content increases, and reaches a maximum for aETI = 4%. We note here that the presence of ETI has a strong impact on the film qualities, even when the optical and structural properties do not seem to be affected, showing an induced stabilization that calls for deeper investigations. Moreover, here we were selectively targeting the thermal degradation of MAPbI3, and thus the equilibrium related to MAI decomposition and out-diffusion from the perovskite film, which seems to be significantly retarded in the presence of the ETI additive. In addition, given the enhanced resistant to moisture we investigated their surface properties by contact-angle (θc) measurements (see the inset of Figure 3c). The results, obtained from the average of 4 different samples, show a clear modification of the surface as the ETI content increases, switching from hydrophilic to hydrophobic with only aETI > 2 % (see also Figure S7). We also monitored the degradation of the materials in air with 50% humidity at room temperature. The results, shown in Figure S8, clearly demonstrate an enhanced stability in the films with 1% ETI, preserving its characteristic dark color after 2 months, as opposed to MAPbI3, which becomes clearly yellow. We note here that increased hydrophobicity has previously been shown to improve perovskite stability, but attributed to an enhanced resistance of the film to moisture. On the contrary, here, the increased hydrophobicity of the ETI: MAPbI3 blends prevent the heat induced out-diffusion of MA, as suggested by the XRD analysis (Figure 3), favoring perovskite stabilization at elevated working temperatures [42]. Noteworthy, such conception concerns all the high-efficiency formulations, as they contain MA as an inherent source of instability, which could be easily retarded by using this facile approach.

In summary, the effect of a hydrophobic IL, ETI, on the photovoltaic performance of PSCs was investigated. By blending the material at low molar concentrations, improvements in both efficiency and thermal stability were observed, mainly due to an enhanced Jsc. Our results suggest that the reduced thermal degradation of the doped films originates from the hydrophobicity of the additive, which behaves as permeation barrier inhibiting the out-diffusion of MA. Exploiting this simple concept allows solar cells with PCE exceeding 19 % to be fabricated, which are endowed with high stabilities at elevated temperatures and in humid conditions. Overall, this study describes a facile and effective approach to retard degradation of MAI containing perovskites, and invites to explore other hydrophobic additives to overcome thermal instability of perovskite formulations.

Supporting Information

Supporting Information is available from the Wiley Online Library or from the author.

Acknowledgements

We thank the EPFL, the Swiss National Science Foundation, and the National Natural Science Foundation of China (11674324 and 11604339) for financial support. We thank Manuel Tschumi for conducting the stability tests and Mounir Mensi for the XPS studies. G. G. acknowledge support from the Swiss National Science Foundation (SNSF), funding through the Ambizione Energy project HYPER (grant number PZENP2_173641

References

[1] NREL Best Research-Cell Efficiencies, www.nrel.gov/ncpv/images/effciency_chart.jpg (accessed: April 2018).

[2] S. De Wolf, J. Holovsky, S.-J. Moon, P. Löper, B. Niesen, M. Ledinsky, F.-J. Haug, J.-H. Yum, C. Ballif, J. Phys. Chem. Lett. 2014, 5, 1035.

[3] S. D. Stranks, G. E. Eperon, G. Grancini, C. Menelaou, M. J. P. Alcocer, T. Leijtens, L. M. Herz, A. Petrozza, H. J. Snaith, Science, 2013, 342, 341.

[4] V. D’Innocenzo, G. Grancini, M. J. P. Alcocer, A. R. S. Kandada, S. D. Stranks, M. M. Lee, G. Lanzani, H. J. Snaith, A. Petrozza, Nat. Commun. 2014, 5, 3586.

[5] D. P. McMeekin, G. Sadoughi, W. Rehman, G. E. Eperon, M. Saliba, M. T. Hörantner, A. Haghighirad, N. Sakai, L. Korte, B. Rech, M. B. Johnston, L. M. Herz, H. J. Snaith, Science 2016, 351, 151.

[6] Y. Wu, A. Islam, X. Yang, C. Qin, J. Liu, K. Zhang, W. Peng, L. Han, Energy Environ. Sci. 2014, 7, 2934.

[7] S. Colella, E. Mosconi, P. Fedeli, A. Listorti, F. Gazza, F. Orlandi, P. Ferro, T. Besagni, A. Rizzo, G. Calestani, G. Gigli, F. D. Angelis, R. Mosca, Chem. Mater. 2013, 25, 4613.

[8] D. Q. Bi , P. Gao, R. Scopelliti, E. Oveisi, J. S. Luo, M. Grätzel, A. Hagfeldt, M. K. Nazeeruddin, Adv. Mater. 2016, 28, 2910.

[9] Y. Z. Wu, F. X. Xie, H. Chen, X. D. Yang, H. M. Su, M. L. Cai, Z. M. Zhou, T. Noda, L. Y. Han, Adv. Mater. 2017, 29, 1701073.

[10] M. I. Asghar, J. Zhang, H. Wang, P. D. Lund, Renew. Sust. Energ. Rev. 2017. 77. 131.

[11] W. R. Mateker, M. D. McGehee, Adv. Mater. 2017, 29, 1603940.

[12] C. J. Qin, T. Matsushima, T. Fujihara, C. Adachi, Adv. Mater. 2017, 29, 1603808.

[13] R. K. Misra, S. Aharon, B. Li, D. Mogilyansky, I. Visoly-Fisher, L. Etgar, E. A. Katz, J. Phys. Chem. Lett. 2015, 6, 326.

[14] G. D. Niu, W. Z. Li, F. Q. Meng, L. D. Wang, H. P. Dong, Y. Qiu, J. Mater. Chem. A 2014, 2, 705.

[15] F. M. Li, M. Z. Liu, J. Mater. Chem. A 2017, 5, 15447.

[16] H.-S. Kim, J.-Y, Seo, N.-G, Park, ChemSusChem. 2016, 9, 2528.

[17] D. Wang, M. Wright, N. K. Elumalai, A. Uddin, Sol. Energy Mater. Sol. Cells 2016, 147, 255.

[18] K. O. Brinkmann, J. Zhao, N. Pourdavoud, T. Becker, T. Hu, S. Olthof, K. Meerholz, L. Hoffmann, T. Gahlmann, R. Heiderhoff, M. F. Oszajca, N. A. Luechinger, D. Rogalla, Y. Chen, B. Cheng, T. Riedl, Nat. Commun. 2017, 8, 13938.

[19] Q. Hu, Y. Liu, Y. Li, L. Ying, T. H. Liu, F. Huang, S. F. Wang, W. Huang, R. Zhu, Q. H. Gong, J. Mater. Chem. A 2015, 3, 18483.
[20] T. M. Koh, J. Huang, I. Neogi, P. P. Boix, S. G. Mhaisalkar, N. Mathews, ACS Appl. Mater. Interfaces 2017, 9, 28743.

[21] T. M. Koh, V. Shanmugam, J. Schlipf, L. Oesinghaus, P. Müller-Buschbaum, N. Ramakrishnan, V. Swamy, N. Mathews, P. P. Boix, S. G. Mhaisalkar, Adv . Mater. 2016, 28, 3653.

[22] D. Pérez-del-Rey, P. P. Boix, M. Sessolo, A. Hadipour, H. J. Bolink, J. Phys. Chem. Lett. 2018, 9, 1041.

[23] A. Bashir, S. Shukla, J. H. Lew, S. Shukla, A. Bruno, D. Gupta, T. Baikie, R. Patidar, Z.Akhter, . Priyadarshi, N. Mathews, S. G. Mhaisalkar, Nanoscale, 2018, 10, 2341.

[24] H. Chen, D. Bryant, J. Troughton, M. Kirkus, M. Neophytou, X. H. Miao, J. R. Durrant, I. McCulloch, Chem. Mater. 2016, 28, 2515.

[25] M. D. Xiao, F. Z. Huang, W. C. Huang, Y. Dkhissi, Y. Zhu, J. Etheridge, A. Gray-Weale, U. Bach, Y. B. Cheng, L. Spiccia, Angew. Chem. Int. Ed. 2014, 53, 9898.

[26] Y. X. Zhao, K. Zhu, J. Phys. Chem. Lett. 2014, 5, 4175.

[27] P.-W. Liang, C.-Y. Liao, C.-C. Chueh, F. Zuo, S. T. Williams, X.-K. Xin, J. J. Lin, A. K.-Y. Jen, Adv. Mater. 2014, 26, 3748.

[28] L. Li, Y. H. Chen, Z. H. Liu, Q. Chen, X. D. Wang, H. P. Zhou, Adv. Mater. 2016, 28, 9862.

[29] J.-Y. Seo, T. Matsui, J. S. Luo, J.-P. Correa-Baena, F. Giordano, M. Saliba, K. Schenk, A. Ummadisingu, K. Domanski, M. Hadadian, A. Hagfeldt, S. M. Zakeeruddin, U. Steiner, M. Grätzel, A. Abate, Adv. Energy Mater. 2016, 1600767.

[30] D. T. Moore, K. W. Tan, H. Sai, K. P. Barteau, U. Wiesner, L. A. Estroff, Chem. Mater. 2015, 27, 3197.

[31] Y. Zhang, Z. F. Fei, P. Gao, Y. H. Lee, F. F. Tirani, R. Scopelliti, Y. Q. Feng, P. J. Dyson, M. K. Nazeeruddin, Adv. Mater. 2017, 1702157.

[32] D. Yang, R. X. Yang, X. D. Ren, X. J. Zhu, Z. Yang, C. Li, S. Z. Liu, Adv. Mater. 2016, 28, 5206.

[33] D. Yang, X. Zhou, R. X. Yang, Z. Yang, W. Yu, X. L. Wang, C. Li, S. Z. Liu, R. P. H. Chang. Energy Environ. Sci. 2016, 9, 3071.

[34] F. Han, J. S. Luo, H. A. Malik, B. W. Zhao, Z. Q. Wan, C. Y. Jia, J. Power Sources 2017, 359 577.

[35] M. Z. Long, T. K. Zhang, H. Y. Zhu, G. X. Li, F. Wang, W. Y. Guo, Y. Chai, W. Chen, Q. Li, K. S. Wong, J. B. Xu, K. Y. Yan, Nano Energy 2017, 33, 485.

[36] T. Leijtens, K. Bush, R. Cheacharoen, R. Beal, A. Bowring, M. D. McGehee, J. Mater. Chem. A 2017, 5, 11483.

[37] Z. Li, J. Tinkham, P. Schulz, M. J. Yang, D. H. Kim, J. Berry, A. Sellinger, K. Zhu, Adv. Energy Mater. 2017, 7, 1601451.

[38] Y. Xie, F. Shao, Y. M. Wang, T. Xu, D. L. Wang, F. Q. Huang, ACS Appl. Mater. Interfaces 2015, 7, 12937.

[39] Y. Z. Wu, A. Islam, X. D. Yang, C. J. Qin, J. Liu, K. Zhang, W. Q. Peng, L. Y. Han, Energy Environ. Sci. 2014, 7, 2934.

[40] H. Zhang, J. Mao, H. X. He, D. Zhang, H. L. Zhu, F. X. Xie, K. S. Wong, M. Grätzel, W. C. H. Choy, Adv. Energy Mater. 2015, 5, 1501354.

[41] A. D. Jodlowski, C. Roldán-Carmona, G. Grancini, M. Salado, M. Ralaiarisoa, S. Ahmad, N. Koch, L. Camacho, G. D. Miguel, M. K. Nazeeruddin, Nat. Energy 2017, 2, 972.

[42] A. Latini, G. Gigli, A. Ciccioli, Sustainable Energy Fuels 2017, 1, 1351.

Figure. 1 (a) Schematic of the PSCs based on MAPbI3 doped with ETI. (b) Cross-sectional SEM image of the typical device based on the 1% ETI doped MAPbI3. (c) UV–vis absorption (left) and PL spectra excited at 500 nm (right) of the MAPbI3 films doped with ETI (0, 1, 2, and 4%) on glass. (d) XRD patterns based on samples of MAPbI3 (doped with different concentrations of ETI)/mp-TiO2/FTO (e) Highlighted diffraction profiles in the 2θ range 12 - 15° of (d). (f) Surface SEM images of MAPbI3 with/without 1% ETI.

Figure. 2 (a) J-V curves, (b) IPCE spectra, and (c) statistical deviation of the photovoltaic parameters obtained for the devices containing perovskite films based on different ETI concentrations (15 solar cells per condition).

Figure. 3 Stability tests performed for the perovskite solar cells based on MAPbI3 and 1% ETI: MAPbI3 performed under (a) MPPT tracking in argon atmosphere at 60 ℃, and (b) ambient air, 40 ± 5% humidity at room temperature. (c) XRD evolution of MAPbI3 films containing different ETI concentrations at 60° in an inert atmosphere. The insets show the contact angle pictures of deionized water dropped on the corresponding perovskite films.

TOC