Swelling-Induced Chain Stretching Enhances Hydrolytic Degrafting of Hydrophobic Polymer Brushes in Organic Media

[*]	J. Wang, Prof. H.-A. Klok
École Polytechnique Fédérale de Lausanne (EPFL)

Institut des Matériaux and Institut des Sciences et Ingénierie Chimiques, Laboratoire des Polymères

Bâtiment MXD, Station 12, CH-1015 Lausanne (Switzerland)
E-mail: harm-anton.klok@epfl.ch

Supporting information for this article is given via a link at the end of the document.

Jian Wang and Harm-Anton Klok*

Abstract: Hydrophilic polymer brushes grown via surface-initiated polymerization from silicon oxide surfaces can detach or degraft in aqueous media. Degrafting of these chain end-tethered polymers is believed to involve hydrolysis of bonds at the polymer – substrate interface. Degrafting so far has not been reported for hydrophobic polymer brushes in non-aqueous media. This study has investigated the degrafting and swelling properties of poly(tert-butyl methacrylate) (PtBMA) brushes in different water-miscible, organic solvents, viz. DMF, acetone and THF. In the presence of a sufficient quantity of water in the organic solvent, degrafting was also observed for PtBMA brushes. More importantly, however, the rate of degrafting depended on the nature of the organic solvent and the apparent initial rate constant of the degrafting reaction was found to correlate with the swelling ratio of the polymer brush in the different solvents. This correlation is first, direct evidence in support of the hypothesis that degrafting is facilitated by a tension that acts on the bond(s) that tether the polymer chains to the surface and which is amplified upon swelling of the polymer brush.

Surface-initiated polymerization (SIP) reactions provide access to chain end-tethered polymer assemblies (“polymer brushes”) in which neighboring polymer chains are anchored at intermolecular distances that enforce a stretched chain conformation.[1] The extended chain conformation is an important contributor to e.g. the nonbiofouling[2] and lubrication properties[3] of hydrophilic polymer brushes prepared by SIP.

Chain stretching in densely grafted polymer brushes also results in a tension that acts on the bonds, which anchor the polymer chains to the underlying substrate. Exposure to a good solvent and swelling of the polymer brush film can amplify this tension. For a number of hydrophilic polymer brushes grown via surface-initiated atom transfer radical polymerization (SI-ATRP) from silicon oxide substrates modified with organosilane functionalized ester or amide based ATRP initiators, incubation in aqueous media results in detachment (degrafting) of the surface-anchored polymer chains.[4] The degrafting of hydrophilic polymer brushes from silicon oxide surfaces in aqueous media has been attributed to a swelling-induced stretching of the surface-anchored polymer chains and a concomitant amplification of the tension that acts on the siloxane and ester/amide bonds that anchor the chains to the surface.[5] The increased tension at the polymer brush-substrate interface has been postulated to facilitate hydrolysis of the anchoring siloxane and ester/amide bonds resulting in the observed degrafting of the surface-attached polymer chains.

The application of tension on the anchoring points of chain end-tethered polymers by swelling-induced chain stretching represents an alternative method to apply force at the molecular level. Other strategies that have been applied to mechanically activate polymers include the use of ultrasound irradiation[6] and flow fields.[7] These methods, however, generate relative strong forces (~ nN) that are sufficient to induce scission of carbon-carbon bonds in a polymer backbone. Carbon – carbon bond scission has also been observed upon adsorption of bottlebrush macromolecules on surfaces.[8] Swelling-induced stretching of chain end-tethered polymers, in contrast, produces weak forces that do not allow direct scission of covalent bonds but is rather believed to mechanically catalyze reactions, such as for example the hydrolysis of the ester/amide and siloxane bonds that typically anchor polymer brushes grown via SI-ATRP.

While it has been proposed that swelling of a polymer brush and the concomitant stretching of the surface-anchored polymer chains enhances hydrolytic cleavage of bonds at the brush-substrate interface, there is so far no experimental data that show a correlation between the swelling properties of a polymer brush and, for example, the initial rate constant of the degrafting reaction. This manuscript studies the swelling properties and degrafting behavior of poly(tert-butyl methacrylate) (PtBMA) brushes (Scheme 1) in organic solvents in the presence of small quantities of water. The use of a hydrophobic brush that swells in a water-miscible organic solvent allows to decouple swelling of the brush and hydrolytic cleavage of the bond(s) at the brush-substrate interface. With hydrophilic brushes in aqueous media this is not possible since in these conditions water simultaneously acts as the solvent that swells the brush and as the reagent that is involved in hydrolytic cleavage. PtBMA brushes can undergo moderate to strong swelling in a range of water-miscible organic solvents. This is attractive as it allows to modulate swelling of the PtBMA brushes, and thus stretching of the surface-grafted polymer chains, at a constant concentration of reagent responsible for the degrafting reaction.

Using the PtBMA brushes as a model system, this manuscript will address several fundamental, open questions related to the degrafting of polymer brushes from silicon oxide substrates. The first question is whether hydrolytic degrafting of polymer brushes occurs exclusively in aqueous media or whether this phenomenon can also be observed in organic media? If degrafting is driven by the increase in tension at the brush-substrate interface as a consequence of chain stretching that results from swelling of the brush, then, in the presence of an appropriate reagent, this process may also occur in organic media (and may also be extended to other cleavage reactions than  hydrolysis). Much of the work on the degrafting of polymer brushes points towards swelling of the brush film as the driving force for tension amplification at the brush-substrate interface and concomitant cleavage of the surface-anchored polymer chains. What is not known and has not been demonstrated yet is whether the rate of degrafting of a polymer brush correlates with its swelling behavior and whether the rate of degrafting can be modulated by varying the degree of swelling of the brush. The PtBMA brushes used in this study are an ideal model system to investigate these questions.

Scheme 1. Preparation of PtBMA brushes via SI-ATRP.

PtBMA brushes were grown by SI-ATRP of tert-butyl methacrylate (tBMA) from 2-bromo-2-methyl-N-{3-[chloro(dimethyl)silyl]-propyl}propanamide modified silicon oxide substrates as shown in Scheme 1 following a modified literature procedure.[9] Degrafting of the end tethered PtBMA chains via hydrolysis of the siloxane or amide bonds that anchor the polymer to the substrate will result in a gradual decrease in the grafting density of the polymer brush (Scheme 2). This will lead to a continuous decrease in the dry film thickness of the PtBMA brushes as the degrafting process proceeds. Degrafting is a process that is driven by the entropy gain associated with the cleavage and release of conformationally restricted, surface-tethered polymer chains. The bond tension in chain end tethered, swollen brushes scales with the inverse of the grafting density and has been estimated to 1-10 pN in a dense brush to 0.1-1.0 pN in the mushroom regime.[10] While these tensions are not sufficient to allow direct scission of covalent bonds, the degrafting of polymer brushes observed by us and others[4] suggests, however, that these may facilitate hydrolytic cleavage of siloxane and/or amide bonds at the polymer brush – substrate interface. As degrafting progresses, the grafting density, and thus the tension at the interface, continuously decreases. Degrafting proceeds to a limiting, non-zero film thickness where this tension is believed to be reduced to a value that is no longer sufficient to facilitate hydrolytic cleavage.[5]

Scheme 2. Schematic illustration of the swelling and subsequent degrafting of a PtBMA brush, resulting in a gradual decrease in grafting density and dry film thickness.

Ellipsometry was used to characterize the swelling behavior of the PtBMA brushes and to monitor the degrafting process. To describe the swelling properties of the PtBMA brushes in the different media, the swelling ratios were determined, which are defined as the ratio of the swollen and dry film thickness of the initial polymer brush. Degrafting was monitored by determining the dry film thickness of the PtBMA brushes at regular time intervals.

In a first set of experiments, PtBMA brushes with an initial dry film thickness of 160 nm were incubated in THF, toluene and water as well as various THF and toluene-water mixtures. The dry film thickness of the samples was monitored for a period of 7 days. Exposure of the PtBMA brushes to dry toluene, toluene + 330 ppm water, THF + 11 ppm water as well as pure water did not reveal any significant changes in dry film thickness (Figure 1A). Apparently, although THF and toluene are good solvents for PtBMA and will swell the brush, the water concentration in these media is too low to facilitate hydrolytic cleavage of the bonds at the brush-substrate interface. Similarly, also no changes in dry film thickness were observed when PtBMA brushes were incubated in dry DMF or dry acetone (Figure S1). Exposure to water was also not found to result in any changes in dry film thickness. Water is a non-solvent for PtBMA. As a consequence, the PtBMA brush does not swell, which limits access of water to the brush-substrate interface and no changes in dry film thickness are observed either. Increasing the amount of water in THF to 5, respectively, 20 vol%, however, results in rapid degrafting (Figure 1B). This illustrates the presence of water as a necessary requirement for degrafting to occur.

The kinetics of diffusion of the cleaved chains through the surface-grafted polymer film do not seem to influence or limit the degrafting process. This is illustrated in Figure S2, which compares the dry film thickness of a PtBMA brush before and after incubation in THF + 5 vol% water for 4 hours. The dry thickness of the PtBMA film that was taken from the degrafting medium after 4 hours was determined both without any further washing steps as well as after washing the brush with various solvents. The results in Figure S2 reveal no significant differences in the dry film thickness that was determined directly after withdrawing the PtBMA film from the incubation medium without further washing and the film thicknesses that were measured after subjecting the brush film to a series of subsequent washing steps using a number of solvents. This indicates that cleavage and subsequent escape of the detached polymer chains is not influenced or limited by diffusion barriers imposed by the remaining, surface-anchored polymer chains.

Gel permeation chromatography (GPC) analysis was used to monitor changes in the molecular weight of the surface-attached polymer chains as degrafting proceeds. Polymer molecular weights were determined by HF-mediated cleavage of the surface-tethered PtBMA, both at t = 0 (before degrafting) as well as after incubation of the brush in THF + 5 vol% water for 4 hours. For a PtBMA brush with an initial dry film thickness of 165 nm, the initial number average molecular weight (t = 0) was 248 kDa. After incubation of this brush in THF + 5 vol% water, the molecular weight of the residual, surface-tethered PtBMA was determined to 231 kDa (Figure S3). This suggests that it is the higher molecular weight fraction that degrafts first, which is in agreement with observations reported in other studies.[4i]

As illustrated in Figure 1B, degrafting is fastest in THF + 5 vol% water and seems to slow down upon increasing the amount of water to 20 vol%. Interestingly, the results in Figure 1B correlate with the swelling properties of the PtBMA brushes in THF-water mixtures (Figure 1D). Whereas the swelling ratio of a 160 nm thick PtBMA brush in THF + 5 vol% water is 3.9 (and similar to the swelling ratio of the brush in dry THF), increasing the water content to 20 vol% is accompanied by a reduction in the swelling ratio to 2.6. The lower swelling ratio of the PtBMA brush in THF + 20 vol% water is consistent with a lower tension at the brush-substrate interface, which concurs with the lower rate of degrafting that is observed in THF + 20 vol% water as compared to THF + 5 vol% water. Figure 1C shows the evolution of dry film thickness as a function of time (over a period of 2 days) upon incubation of PtBMA brushes with initial dry film thicknesses of 50, 80 and 160 nm in THF + 5 vol% water. Figure S4 shows the change in dry film thicknesses of these brushes over a period of 7 days. The initial swelling ratios of the PtBMA brushes are also included in Figure 1D. The swelling ratios of PtBMA brushes of different film thicknesses were also determined by AFM analysis of micropatterned samples.[11] The results of these experiments are included in Figure S5 and are in good agreement with the swelling ratios reported in Figure 1D.

Figure 1. Ellipsometric dry thickness of PtBMA brushes as a function of incubation time upon exposure to: (A) Toluene (■), THF + 11 ppm water (●), Toluene + 330 ppm water (▲), pure water (▼); (B) THF + 11 ppm water (■), THF + 5 vol% water (▲), THF + 20 vol% water (●); (C) Evolution of the dry film thickness of PtBMA brushes with initial dry film thicknesses of 160 nm (▲), 80 nm (●) and 50 nm (■) upon incubation in THF + 5 vol% water; (D) Swelling ratios measured by ellipsometry of PtBMA brushes of initial dry film thicknesses of 50, 80 and 160 nm in water (black), THF + 20 vol% water (red), THF + 5 vol% water (blue) and THF (pink).

To quantitatively describe the degrafting of the PtBMA brushes and evaluate the influence of the composition of the solvent and the initial dry film thickness, Figure 1B and Figure 1C were replotted as ln (d) versus time (Supporting information Figure S6). The ln (d) versus time plots reveal 2 linear regimes, suggesting that the degrafting process follows a pseudo-first order kinetics. The slope of the first linear regime was taken as the apparent, initial rate constant (kini) of the degrafting process. Figure 2A shows kini and the initial swelling ratio for a PtBMA brush with an initial dry film thickness of 160 nm in THF, THF + 5 vol% water and THF + 20 vol% water. In Figure 2B, the kini and initial swelling ratios for PtBMA brushes with initial dry film thicknesses of 50, 80 and 160 nm in THF + 5 vol% water are summarized. The results in Figure 2A suggest a correlation between the swelling ratio, i.e. chain stretching and tension at the bonds at the brush-substrate interface and the kini. Upon decreasing the amount of water in THF from 20 vol% to 5 vol%, the initial swelling ratio increases from 2.6 to 3.9. This increase in swelling ratio is accompanied by an increase in kini from 0.7 d-1 to 2.9 d-1. As indicated in Figure 2B, the initial swelling ratio of PtBMA brushes in THF + 5 vol% water did not significantly change upon varying the dry film thickness from 50 to 160 nm. Consistent with this observation, the kini values measured for PtBMA brushes in THF + 5 vol% water were also not found to depend on the initial dry film thickness.

Figure 2. (A) Initial rate constant of degrafting (left) and initial swelling ratio (right) for PtBMA brushes with an initial dry film thickness of 160 nm upon incubation in THF, THF + 5 vol% water and THF + 20 vol% water; (B) Initial rate constant of degrafting (left) and initial swelling ratio (right) determined for PtBMA brushes with initial dry film thickness of 50, 80 and 160 nm in THF + 5 vol% water.

The results presented in Figure 2 provide a first indication that the kini, and thus the putative tension at the brush-substrate interface, correlates with the swelling ratio of the polymer brush. To vary the swelling of the PtBMA brushes in these experiments, the relative amounts of THF and water were varied. To vary the swelling of the PtBMA brush while keeping the water concentration constant, a second series of degrafting experiments with 3 different water-miscible organic solvents, viz DMF, acetone and THF was carried out. For these experiments, PtBMA brush samples with an initial dry film thickness of ~160 nm were used, which were incubated in mixtures of the different organic solvents that contained 5 vol% water. Figure 3A shows the evolution of the dry film thickness of the brushes as a function of time upon incubation in the different media. These data were analyzed in the same way as discussed above to determine the kini for the degrafting of the PtBMA brushes (Supporting information Figure S7). Figure 3B presents kini and the initial swelling ratios of the PtBMA brushes in the 3 different media. Upon changing the incubation medium from DMF + 5 vol% water to acetone + 5 vol% water to THF + 5 vol% water, kini increased from 0.003 d-1 to 0.226 d-1 to 2.944 d-1. Swelling of the PtBMA brushes in these media follows the same trend. The swelling ratios of the PtBMA brushes increased from 1.4 in DMF + 5 vol% water to 2.3 in acetone + 5 vol% water to 3.9 in THF + 5 vol% water. These results corroborate those shown in Figure 2 and indicate that kini, and thus the putative tension that acts on the bonds at the brush-silicon oxide interface, correlates with the extent of swelling of the surface grafted polymers.

Figure 3. (A) Evolution of dry film thickness of a PtBMA brush with an initial thickness of 160 nm upon exposure to DMF + 5 vol% water (■), acetone + 5 vol% water (●) and THF + 5 vol% water (▲); (B) Initial rate constant of degrafting (left) and swelling ratio (right) determined for a PtBMA brush with an initial dry film thickness of 160 nm in DMF + 5 vol% water, THF + 5 vol% water and acetone + 5 vol% water.

In a final set of experiments, degrafting of PtBMA brushes with initial grafting densities of 100%, 50% and 20% was investigated. These brushes were prepared by SI-ATRP of tBMA from silicon oxide surfaces that were modified with mixtures of the ATRP active 2-bromo-2-methyl-N-{3-[chloro(dimethyl)silyl]-propyl}propanamide and the polymerization inactive “dummy” N-(3-(chlorodimethylsilyl)propyl)pivalamide, which contained 100 mol%, 50 mol% or 20 mol% of the ATRP initiating organosilane. From these substrates, which present different ATRP initiator surface concentations, PtBMA brushes were grown using a polymerization time of 0.5 h. For a silicon oxide substrate modifed with 100 mol% of the ATRP active chlorosilane this results in a dry film thickness of 160 nm. Degrafting of this series of PtBMA brushes was studied in DMF, acetone and THF, all in the presence of 5 vol% water. The kini, which were obtained from the decrease in dry film thickness as a function of incubation time, are summarized in Figure 4A for brushes of different initial grafting densities and the different degrafting media (Figure S8 presents the corresponding ln (d) versus time plots). Figure 4B compares the ratio of kini for degrafting in THF + 5 vol% water and acetone + 5 vol% water for PtBMA brushes of initial grafting densities of 20, 50 and 100%. Upon decreasing the grafting density from 100% to 50% to 20%, the ratio kini,THF/kini,acetone decreases from 13 to 9.6 to 1.6. The observed changes in kini,THF/kini,acetone are a strong indication that the differences in kini that are observed in DMF, acetone and THF are not (solely) due to solvent effects, but that chain stretching (and thus tension amplification), in particular at high grafting densities and in good solvents, is a mechanochemical contributor that accelerates the degrafting process. The increases in kini and kini,THF/kini,acetone with increasing grafting density that are shown in Figure 4 are also opposite to what would be expected if access and diffusion of water to the siloxane and amide bonds at the brush – substrate interface would be rate determining.

Results from model studies that have been published on the hydrolysis of tetramethoxysilane (TMOS) and of amides provide further indications for a mechanochemical contribution of swelling-induced chain stretching to the degrafting of polymer brushes grafted from silicon oxide. In experiments, which compared the hydrolysis of TMOS in various solvents, similar reaction rates were observed in a variety of polar, aprotic solvents.[12] Model studies that investigated the base and acid catalyzed hydrolysis of esters and amides have found that reaction rates increase with increasing dielectric constant of the solvent (for the three solvents used in the present study, the dielectric constant is lowest for THF and highest for DMF).[13]

Figure 4. (A) Initial rate constants of degrafting determined for PtBMA brushes with initial grafting densities of 20%, 50% and 100% in DMF + 5 vol% water (black), acetone + 5 vol% (red) water and THF + 5 vol% water (blue) (as the corresponding kini values are very small, the data for DMF + 5 vol% water are not visible); (B) The ratio of kini for degrafting in THF + 5 vol% water and acetone + 5 vol% water for PtBMA brushes of initial grafting densities of 20, 50 and 100%.

The aim of this study was to investigate the swelling-induced, degrafting of hydrophobic polymer brushes grafted by SI-ATRP from planar silicon oxide surfaces in nonaqueous media. The experiments presented here show that in the presence of the appropriate reagent (here: water) degrafting can also be observed for hydrophobic brushes in non-aqueous media. More importantly, the results indicate that degrafting can be modulated by changing the incubation medium and that kini of the degrafting process correlates with the swelling ratio of the polymer brush in the degrafting medium. The correlation between kini and the swelling ratio supports the hypothesis that the degrafting of polymer brushes is driven by an amplification of tension at the polymer brush-substrate interface that is the consequence of swelling of the surface-grafted polymer film. These insights add to the current understanding of the degrafting of polymer brushes and provide a step forward to unravel the parameters that drive this mechanochemical process. The results of this study, however, are not only of interest from a fundamental point of view, but could also impact the technical use of these polymer films and contribute to the design of more robust polymer brushes or to systems that take advantage of this phenomena and harness degrafting in a productive manner, e.g. towards the development of mechanoresponsive surfaces.[14]

Acknowledgements

This work was financially supported by the Swiss National Science Foundation (SNSF) and the China Scholarship Council (No. 201506360078).

Keywords: Degrafting • Hydrolysis reaction • Mechanochemistry • Polymer brushes • Solvent effects

- a) S. Milner, Science 1991, 251, 905; b) B. Zhao, W. J. Brittain, Prog. Polym. Sci. 2000, 25, 677; c) S. Edmondson, V. L. Osborne, W. T. S. Huck, Chem. Soc. Rev. 2004, 33, 14; d) Y. Tsujii, K. Ohno, S. Yamamoto, A. Goto, T. Fukuda, Adv. Polym. Sci. 2006, 197, 1; e) R. Barbey, L. Lavanant, D. Paripovic, N. Schüwer, C. Sugnaux, S. Tugulu, H.-A. Klok, Chem. Rev. 2009, 109, 5437; f) J. O. Zoppe, N. C. Ataman, P. Mocny, J. Wang, J. Moraes, H.-A. Klok, Chem. Rev. 2017, 117, 1105; g) G. Xie, A. Khabibullin, J. Pietrasik, J. Yan, K. Matyjaszewski, Polymer and Biopolymer Brushes: For Materials Science and Biotechnology, Vol. 1 (Eds.: O. Azzaroni, I. Szleifer), John Wiley & Sons Inc, Hoboken, New Jersey, 2018, pp. 29-95; h) W. J. Brittain, S. Minko, J. Polym. Sci., Part A: Polym. Chem. 2007, 45, 3505; i) P. Jain, G. L. Baker, M. L. Bruening, Annu. Rev. Anal. Chem. 2009, 2, 387; j) C. J. Galvin, J. Genzer, Prog. Polym. Sci. 2012, 37, 871; k) O. Azzaroni, J. Polym. Sci., Part A: Polym. Chem. 2012, 50, 3225; l) M. Krishnamoorthy, S. Hakobyan, M. Ramstedt, J. E. Gautrot, Chem. Rev. 2014, 114, 10976; m) C. M. Hui, J. Pietrasik, M. Schmitt, C. Mahoney, J. Choi, M. R. Bockstaller, K. Matyjaszewski, Chem. Mater. 2013, 26, 745; n) B. Li, B. Yu, Q. Ye, F. Zhou, Acc. Chem. Res. 2014, 48, 229; o) L. Wu, U. Glebe, A. Bӧker, Polym. Chem. 2015, 6, 5143; p) W.-L. Chen, R. Cordero, H. Tran, C. K. Ober, Macromolecules 2017, 50, 4089.

- a) A. Hucknall, S. Rangarajan, A. Chilkoti, Adv. Mater. 2009, 21, 2441; b) I. Banerjee, R. C. Pangule, R. S. Kane, Adv. Mater. 2011, 23, 690; c) W. J. Yang, K.-G. Neoh, E.-T. Kang, S. L.-M. Teo, D. Rittschof, Prog. Polym. Sci. 2014, 39, 1017; d) L. Moroni, M. K. Gunnewiek, E. M. Benetti, Acta Biomater. 2014, 10, 2367; e) S. Lowe, N. M. O'Brien-Simpson, L. A. Connal, Polym. Chem. 2015, 6, 198.

- a) P. Mocny, H.-A. Klok, Mol. Syst. Des. Eng. 2016, 1, 141; b) J. Klein, Friction 2013, 1, 1; c) T. Kreer, Soft Matter 2016, 12, 3479; d) E. M. Benetti, M. Divandari, S. N. Ramakrishna, G. Morgese, W. Yan, L. Trachsel, Chem. Eur. J. 2017, 23, 12433; e) G. Morgese, E. M. Benetti, M. Zenobi‐Wong, Adv. Healthcare Mater. 2018, 1701463.

- a) S. Tugulu, H.-A. Klok, Biomacromolecules 2008, 9, 906; b) D. Paripovic, H.-A. Klok, Macromol. Chem. Phys. 2011, 212, 950; c) R. Quintana, M. Gosa, D. Jańczewski, E. Kutnyanszky, G. J. Vancso, Langmuir 2013, 29, 10859; d) E. D. Bain, K. Dawes, A. E. Özçam, X. Hu, C. B. Gorman, J. Šrogl, J. Genzer, Macromolecules 2012, 45, 3802; e) C. J. Galvin, E. D. Bain, A. Henke, J. Genzer, Macromolecules 2015, 48, 5677; f) B. Lego, W. G. Skene, S. Giasson, Macromolecules 2010, 43, 4384; g) Y. Zhu, B. e. Lv, P. Zhang, H. Ma, Chem. Commun. 2011, 47, 9855; h) K. Enomoto, S. Takahashi, T. Iwase, T. Yamashita, Y. Maekawa, J. Mater. Chem. 2011, 21, 9343; i) K. A. Melzak, K. Yu, D. Bo, J. N. Kizhakkedathu, J. L. Toca-Herrera, Langmuir 2015, 31, 6463.

- a) H.-A. Klok, J. Genzer, ACS Macro lett. 2015, 4, 636. b) N. C. Ataman, H.-A. Klok, Macromolecules 2016, 49, 9035.

- P. A. May and J. S. Moore, Chem. Soc. Rev. 2013, 42, 7497.

- a) M. M. Caruso, D. A. Davis, S. Q. Qilong, S. A. Odom, N. R. Sottos, S. R. White, J. S. Moore, Chem. Rev. 2009, 109, 5755. b) K. M. Wiggins, J. N. Brantley, C. M. Bielawski, Chem. Soc. Rev. 2013, 42, 7130.

- a) S. S. Sheiko, F. C. Sun, A. Randall, D. Shirvanyants, M. Rubinstein, H. i. Lee, K. Matyjaszewski, Nature 2006, 440, 191. b) Y. Li, S. S. Sheiko, Top. Curr. Chem. 2015, 369, 1

- Z. Bao, M. L. Bruening, G. L. Baker, J. Am. Chem. Soc. 2006, 128, 9056.

- S. S. Sheiko, S. Panyukov, M. Rubinstein, Macromolecules 2011, 44, 4520.

- S. Tugulu, M. Harms, M. Fricke, D. Volkmer, H.-A. Klok, Angew. Chem. Int. Ed. 2006, 45, 7458; Angew. Chem. 2006, 118, 7619.

- T. W. Zerda, G. Hoang, Chem. Mater. 1990, 2, 372.

- K. J. Laidler, P. A. Landskroener, Trans. Farad. Soc. 1956, 52, 200.

- a) R. Groote, R. T. M. Jakobs, R. P. Sijbesma, Polym. Chem. 2013, 4, 4846; b) J. Li, C. Nagamani, J. S. Moore, Acc. Chem. Res. 2015, 48, 2181; c) B. H. Bowser, S. L. Craig, Polym. Chem. 2018, 9, 3583.

Entry for the Table of Contents (Please choose one layout)

Layout 1:

| COMMUNICATION |  |  |  |  |
| --- | --- | --- | --- | --- |
| Poly(tert-butyl methacrylate) brushes grown from silicon oxide surfaces undergo degrafting upon exposure to water-containing organic solvents. The apparent rate constants of the degrafting reaction are found to correlate with the swelling ratio of the polymer brush in the respective medium. These findings support the hypothesis that degrafting is a mechanochemical process driven by a tension at the polymer – substrate interface, which is amplified upon swelling of the polymer brush in an appropriate solvent. {} |  |  |  | Jian Wang, Harm-Anton Klok* Page No. – Page No. Swelling-Induced Chain Stretching Enhances Hydrolytic Degrafting of Hydrophobic Polymer Brushes in Organic Media |