## Slide 1
Experimental Behavior and Nonlinear Modeling of iron-based Shape Memory
Alloys (SMAs) under Inelastic Cyclic Straining
Heredia Diego (Master’s student)
Resilient Steel Structures Laboratory (RESSLab), Swiss Federal Institute of Technology, Lausanne (EPFL)
1. Objectives
2. Experimental campaign
4.Extendend model for cyclic loading
3. State-of-art material model
Acknowledgments
Loading functions:
Thermomechanical loading representative of those used to prestress concrete
- Conduct an experimental campaign in order to characterize the behavior of Fe-SMAs under cyclic tension/compression straining
  Literature is lacking information on the specificities of Fe-SMAs under cyclic tension/compression straining.
  Tests on Fe-SMAs involving high compressive strains and high strain rates have never been conducted before.
- Implement a state-of-art material model for Fe-SMAs to represent the behavior of such alloys under monotonic tensile loading
  Establish the fundamental equations used in the model that will be used as a starting point to integrate cyclic loading effects.
- Extend the implemented material model to account for cyclic loading
  A constitutive model that can represent all relevant deformation mechanism active in Fe-SMAs is essential to develop and analyze dissipation devices with this material.
Detailed view of the specimen
Round bar coupon
Experimental setup
Prof. Dr. Dimitrios G. Lignos
Dr. Albano de Castro e Sousa
Alexander Hartloper
MTS extensometer
PT100
Temperature at the surface of the specimen
Temperature-strain LP5_SR
(0.03 %/sec)
Temperature-strain LP5_MR
(0.8 %/sec)
Temperature-strain LP5_FR
(8 %/sec)
Hardening is strain rate and/or temperature dependent
Stress-strain LP5_SR
(0.03 %/sec)
Stress-strain LP5_MR
(0.8 %/sec)
Stress-strain LP5_FR
(8 %/sec)
Stress-strain response in compression is characterized by three distinct slopes at low strain
Stress-strain LP2
Stress-strain LP5 (first cycle)
Stress-strain LP7
1
2
3
Comparison with structural steels
Stress-strain LP1
(S690QL and Fe-SMA)
Stress-strain LP5_SR
(S690QL and Fe-SMA)
Stress-strain LP5_SR
(S355J2 and Fe-SMA)
  The maximum tensile strength of the Fe-SMA is similar to the one of a S690QL steel.
  The potential for energy dissipation trough inelastic straining of the Fe-SMA is similar to the one of a S355J2 steel and 1.5 times smaller than the one of a S690QL steel.
Cissé et al. (2017) constitutive model for monotonic tensile loading of Fe-SMAs
  Loading functions:
  Results at T=45°C, phase change and plasticity are coupled:
Stress-strain for different Hs
Evolution of p with Hs
Evolution of ξ with Hs
Stress-strain and stress-temperature of the thermomechanical loading, from Ghafoori et al. (2017)
Stress-strain
Stress-temperature
Evolution of ξ
50 MPa
50 MPa
50 MPa