LONG TERM EFFECT OF MODIFIED BINDER ON CRACKING RESISTANCE OF PAVEMENTS

Prof. A.-G. Dumont1 and M. Ould-Henia1

(1) Laboratory of Traffic Facilities, Swiss Federal Institute of Technology, Lausanne, Switzerland

Abstract

Combined loading and climatic effects associated with the choice of high modulus bituminous mixtures, in order to prevent the pavements from rutting, have increased the risk of cracking failure in the bituminous layers.

It was decided, in 1989, to start a long-term assessment of a wide range of new products. Cracking, rutting and ravelling monitoring have been carried out regularly during 14 years of pavement service. 16 test sections of 300 meters were constructed. The structures of all those test sections were identical, except the choice of the wearing course binder for which 12 modified binders, and 4 pure bitumens as reference, were selected.

A new assessment method of in situ cracking is proposed which consider the gravity and the extent separately in order to get a cracking amplitude parameter. Distinction has been made between the initiation and the propagation of cracking.

In general, PmBs show some improvement of the performance of the wearing course compared to conventional binders. However, one section with direct refining pure bitumen performs as well as some PmBs. Cracking resistance for one section with SBS modified bitumen was tremendous.

A large amount of tests have been carried out on the wearing course binders and mixes during the whole monitoring period. It was noted that classical laboratory tests couldn't be used as tools for the long term behaviour prediction. Thorough studies were carried out on the TSRST, the BBR tests.

# Introduction and goal

Modified binders began to be used extensively about thirty years ago with the aim of improving the mechanical performance of bituminous pavements. This development came in response to traffic increase, on the one hand, but also in order to decrease maintenance periods, which are a major source of traffic disturbance and which, directly or indirectly, lead to additional costs.

At the end of the 1980’s, the Highways Department of the Canton of Valais and the Laboratory for Traffic Facilities (LAVOC) at the Swiss Federal Institute of Technology (EPFL) participated in the preparation of Swiss recommendations concerning polymer modified binders. However, limited information based on experience was available at that time in spite of the use of such products for many years. In 1988, the National Roadway Service of the Canton of Valais constructed the superstructure and the pavement of the N9 motorway over a distance of 15 km. One stretch was made available for the execution of test sections in order to compare the behaviour of polymer and additive modified bituminous mixtures with that of pure bituminous mixtures. A large observation field with identical conditions was made available for the construction of 16 different test sections, each 300 m long. Twelve modified and four pure bitumens, as references, were selected for the construction of the wearing course.

The main goal of the study was the evaluation of the performance and the cost effectiveness of polymer modified bitumen mixtures compared to pure bitumen mixtures. Then, this study aimed the selection of binder or mixture properties to predict long term performance by carrying out conventional and new testing procedures.

In order to assess the long term evolution of the test sections behaviour, many monitoring campaigns and laboratory tests were carried out during the lifetime of the pavement and especially on the wearing course.

# Test sections and monitoring

The pavement was designed according to the Swiss standard SN 640322 of 1971 for a lifetime of 20 years, 1600 ESAL of 8 tons and an annual traffic progression of 5%. All the test sections have the same structure geometry and materials except the binder of the wearing course.

The binder suppliers were invited to propose their recommendations for the design of their binder mixtures; in spite of this all the wearing courses have the same binder content and the same thickness of 4 cm.

The binders’ description is summarised in Table 1:

Table 1 – Type of used binders

|  |  | Type of polymer | Binder category |
| --- | --- | --- | --- |
| Section n° | Base bitumen | Ready to use bitumen | Additives |  |
| 1 | B 80/100 partially blown bitumen + adhesion agent |  |  | pure |
| 2 | B 60/70 partially blown bitumen + adhesion agent |  |  | pure |
| 3 | B 80/100 direct refining | S.B.S. 3% |  | modified |
| 4 | B 40/50 direct refining | S.B.S. 3% |  | modified |
| 5 | B 80/100 direct refining | S.B.S. 5% |  | modified |
| 6 | B 40/50 direct refining | S.B.S. 5% |  | modified |
| 7 | B 80/100 direct refining | Polyolefin 6% |  | modified |
| 8 | B 60/70 direct refining | (polyisobutylen +E.V.A) 11,5% |  | modified |
| 9 | B 60/70 + oxidising agent | E.P.D.M. 4% |  | modified |
| 10 | B 80/100 partially blown bitumen |  | polyolefin 7% | with additives |
| 11 | B 80/100 direct refining | S.B.S. 3% |  | modified |
| 12 | B 80/100 partially blown bitumen |  | (S.B.S. + E.V.A. + agents) 4% | with additives |
| 13 | B 80/100 partially blown bitumen |  | (natural asphalt + filler) 3,6% | with additives |
| 14 | B 80/100 partially blown bitumen (2 steps process.) +B200 | E.P.D.M. 5% |  | modified |
| 15 | B 80/100 direct refining |  |  | pure |
| 16 | B 60/70 direct refining |  |  | pure |

Surface cracking monitoring was done regularly during the lifetime of the sections. Four auscultations were carried out at 4, 7, 10 and 14 years (before overlaying). Beside that, a large laboratory testing program was undertaken to give some indications on materials behaviour so predictive procedures could be established.

Laboratory tests included conventional and “advanced” test procedures on binders and mixtures. Different assessment ages for in-place mixtures were chosen (0, 4 and 8 years). Mixtures and binders taken at the mixing plant were subjected to accelerated aging (DIN, RTFOT and PAV procedures).

# Methodology of cracking assessment

The cracking assessment, according to the Swiss standard SN 640 925, defines two parameters that have to be surveyed: The extent and the gravity of cracking

The extent of cracking (A) is the relative area of sections where cracking is observed (Table 2).

Table 2 – Cracking extent evaluation

| Extent value (A) | Description | % of section concerned |
| --- | --- | --- |
| 0 | no cracking | 0 |
| 1 | very localised | < 10% |
| 2 | localised to extensive | 10..50% |
| 3 | very extensive | > 50% |

The gravity of cracking (S) is 3 for a crack width larger than 10mm, 2 for a crack width between 2 and 10mm and 1 for a crack width smaller than 2mm. The observed cracking is generally smaller than 2mm. Thus, an intermediate evaluation scale was proposed as shown in Table 3.

Table 3 – Cracking extent evaluation

| Gravity value (S) | Type of cracking |
| --- | --- |
| 0.125 | Crack initiation |
| 0.25 | Small isolated cracks |
| 0.75 | Small cracks with some ramifications |
| 1 | Small cracks with dense ramification |

## Cracking amplitude index

The “cracking amplitude index” is defined as the combination of the extent and the gravity values. The product of the two values is normalised and expressed as a percentage. The cracking amplitude index formula is proposed as follow:

ICrack = ( A x S / 9 ) x 100	(1)

The 100% value corresponds to the worst cracking case: 3 for extent and for gravity.

## Cracking propagation threshold

Further more in this paper, two assumptions are made:

- First, the “small isolated cracks” which are “localised to extensive” are considered as a macrostructural indication of cracking initiation on the road surface.

- Then, the cracking going toward some ramification could be considered as an indication of cracking propagation.

These two assumptions allow the definition of a threshold value separating the initiation and the propagation phases. The stage described in the first assumption corresponds to a “cracking amplitude index” calculated hereafter:

ITransition = (2x0.25)/9x100 = 5.6%. (Rounded to 5%)

The year for which the cracking amplitude index exceeds the 5% value is considered as the start of the propagation phase. This parameter called the “transition year” is calculated for all the sections.

Fig. 1 – Cracking amplitude indexes evolution for some test sections

Fig. 2 – Transition years of test sections

# Predictive aspect of laboratory tests versus cracking data

The data collected from laboratory testing and sections monitoring were subjected to a statistical treatment to reveal the significant correlations in order to propose a predictive approach for long term cracking. The following correlations were obtained by a linear regression analysis. Hereafter, only relevant correlations are exposed.

## Correlations on binder properties

The investigations were carried out on all binders except those used in mixtures with additives for evident reasons. As a result, two testing procedures seem to be in accordance with the amplitude of cracking after 10 years: The dynamic viscosity (@ 130 or 150°C) and the Bending Beam Rheometer test.

The dynamic viscosity test was done at different stages of the road construction.  The relative evolution of the dynamic viscosity value between the delivery time and the laying of the mixture was calculated (fig 3) as follow:

IDV  = 1 - ( (laying / (delivery )	(2)

Fig. 3 – Cracking amplitude index at 10 years versus the relative evolution of dynamic viscosity at 150°C between the delivery and the laying stages

This predictive aspect could be explained by the fact that the viscosity increase is due to the progressive loss of oily fractions of bitumen. The binder becomes more brittle, and thus more susceptible to cracking in the mixture.

The BBR test was carried out on extracted binder immediately after laying. The m-value gives also a good correlation with monitored data (fig 4).

Fig. 4 – Cracking amplitude index at 10 years versus the BBR m-value

## Correlations on mixture properties

Analyses were carried out on all mixtures at different aging stages. The most relevant correlation with monitored data was obtained by the Thermal Stress Restrained Specimen Test “TSRST” and its transition temperature value (fig 5). This result was expected considering that this test was used to validate the BBR test.

Fig. 4 – Cracking amplitude index at 10 years versus the TSRST transition temperature

# Conclusions and discussions

The investigations carried out on selected binders and on cracking monitoring data for 14 years permit to issue the following conclusions:

- The test section 11 exhibits a tremendous behaviour. The binder is a widely commercialised product with S.B.S polymer content. After 14 year, no cracking was observed. Test sections 3 and 15 show the same performance at a lower level. The performance of test section 15, containing pure bitumen, is a surprising result.

- For the sections containing pure bitumen (sections 1,2,15,16) a better behaviour is noted for direct refining bitumen sections (15,16). Hence, this way of bitumen processing supplanted the old partial blowing process, improving therefore mixture behaviour. Obviously, the softer is the binder the better is the cracking resistance.

- The sections containing bitumen with polymer additives (sections 10 and 12) do not perform as well as sections with “ready to use” Pmb. This observation could be explained by the fact that polymer bitumen processed in refinery with optimised curing conditions and raw materials properties give a homogeneous and compatible binder with an optimal micro-morphology and thus a better behaviour.

- Two sections (8 and 9), containing respectively polyisobutylen and oxidising agents, give the worse behaviour. The cracking is rather due to chemical aging than to mechanical or thermal cracking.

The correlations between laboratory testing results and cracking amplitudes at 10 years show the following facts:

- The viscosity increase after laying seems to be a good indication of cracking susceptibility.

- The Bending Beam Rheometer m-value is in accordance with the cracking amplitude index.

- Thermal Stress Restrained Specimen Test carried out on mixtures which were cored after the laying shows a good correlation between the test transition temperature and the observed cracking.

# Acknowledgment

The sections monitoring and laboratory work was funded by the Swiss federal Roads Authority and the Highway Department of the Canton of Valais. The cooperation of these agencies permitted a good assessment of the test sections during the whole lifetime of the structures.

# References

- Dumont A.-G., Huet M., Simond E., "Vieillissement de bitumes modifiés issus de planches comparatives réalisées en Suisse, dans le canton du Valais", Congrès Eurobitume, Stockholm juin 1993

- Dumont A.-G., Turtschy J.-C., Scazziga I., Pucci T., Fontana M., "Analyse des modèles de comportement des chaussées", Rapport OFR n°1002, juillet 2001

- Dumont A.-G., Schwery B., Angst Ch., "Planches comparatives avec bitumes modifiés et ajouts", Rapport OFR n°1035, septembre 2002

- Performance analysis of road Infrastructure (PARIS) , final report, November 1998

- Pucci T., "Approche prévisionnelle de la fissuration par sollicitation thermique des revêtements bitumineux", thèse de doctorat, Ecole Polytechnique Fédérale de Lausanne, Suisse, octobre 2001

- Vinson Ted S., Janoo V.C., Haas Ralph C.G., "Low temperature and thermal fatigue cracking", Summary Report SR-OSU-A-003A-89-1, Strategic Highway Research Program contract A-033A, 1989

- Vinson Ted S., Kanerva H.K., Zeng H, "Low temperature cracking: field validation of the Thermal Stress Restrained Specimen Test (TSRST)", Strategic Highway Research Program SHRP-A-401 contract A-033A, Washington DC 1994