Large scale inkjet-printing of carbon nanotubes electrodes for antioxidant assays in blood bags

- Electronic supporting information -

Andreas Lesch,a Fernando Cortés-Salazar,a Michel Prudent,b Julien Delobel,b Shokoufeh Rastgar,c Niels Lion,b Jean-Daniel Tissot,b Philippe Tacchinid and Hubert H. Giraulta,*

a Ecole Polytechnique Fédérale de Lausanne, Laboratoire d’Electrochimie Physique et Analytique, Station 6, CH-1015 Lausanne, Switzerland

b Service Régional Vaudois de Transfusion Sanguine, Unité de Recherche et Développement, CH-1066 Epalinges, Switzerland

c Department of Chemistry, Sharif University of Technology, Tehran 11155-9516, Iran.

d Edel for Life, PSE-B/EPFL, CH-1015 Lausanne, Switzerland

* CORRESPONDING AUTHOR FOOTNOTE

EMAIL:			hubert.girault@epfl.ch

Telephone number:		+41 (0)21 693 31 51

Fax number: 			+41 (0)21 693 36 67

SI-1 Laser scanning microscopy and scanning electron microscopy of the inkjet-printed carbon nanotubes electrodes

Figure SI-1. a) Laser scanning micrograph of a 4-IJPL CNT pattern on polyimide (PI). b) Scanning electron micrograph of a 4-IJPL CNT pattern on Ag and PI substrate.

SI-2 Cyclic voltammetry of the inkjet-printed carbon nanotubes electrodes

Figure SI-2. Cyclic voltammetries (CVs, first cycle) in 2 mM FcMeOH using one 1-IJPL CNT sensor (a) and one 4-IJPL CNT sensor (b). Various scan rates ν in mV·s-1: 10, 25, 50, 100, 250, 500, 1000.

Figure SI-3. Baseline-corrected anodic peak current Ipa vs. the square root of the scan rate (ν1/2) for 1-IJPL, 2-IJPL and 4-IJPL CNT sensors. Electrolyte solution: 2 mM FcMeOH in 0.1 M KCl.

SI-3 Randles-Sevcik equation

The Randles-Sevcik equation is as follows,

The Randles-Sevcik equation at room temperature can be written as:

Am – microscopic electrode area (cm2)

ipa – anodic peak current in (A)

n – number of transferred electrons

D – diffusion coefficient of the redox mediator (cm2·s-1)

ν – scan rate (V·s-1)

c* – concentration of the redox mediator in bulk solution (mol·cm-3)

SI-4 Variation of λ and Ethreshold in the pseudo-titration voltammetry

Figure SI-4. Effect of adjusting λ and Ethreshold in the pseudo-titration process.