DOI: 10.1002/((please add manuscript number))

Article type: Communication

Picosecond Capture of Photoexcited Electrons improves Photovoltaic Conversion in MAPbI3:C70 doped Planar and Mesoporous Solar Cells

Saba Gharibzadeh a,b, Franco Valduga de Almeida Camargo  c, Cristina Roldán-Carmona a, Grégoire Clément Gschwend d, Jorge Pascual e,f, Ramón Tena-Zaera e, Giulio Cerullo c, Giulia Grancini a,*, Mohammad Khaja Nazeeruddin a,*

a S. Gharibzadeh, Dr. C. Roldán-Carmona, Dr. G. Grancini, Prof. Md. K. Nazeeruddin, Group for Molecular Engineering of Functional Materials, Ecole Polytechnique Fédérale Lausanne Valais Wallis, Sion CH-1951, Switzerland

b S. Gharibzadeh, Department of Physics, Tarbiat Modares University, P.O. Box 14115-175, Tehran-Iran

c Dr. F. Valduga de Almeida Camargo, Prof. G. Cerullo, Istituto di Fotonica e Nanotecnologie del CNR, Dipartimento di Fisica, Politecnico di Milano, P.zza L. da Vinci 32, 20133 Milano, Italy
d LEPA, Ecole Polytechnique Fédérale Lausanne Valais Wallis, Sion CH-1951, Switzerland

e J. Pascual, Dr. R. Tena-Zaera, IK4-CIDETEC, Parque Tecnológico de San Sebastián, Paseo Miramón 196, Donostia-San Sebastián 20009, Spain

f J. Pascual POLYMAT, University of the Basque Country UPV/EHU

Avenida de Tolosa 72, Donostia-San Sebastián 20018, Spain

Hybrid Perovskite solar cells, C70:MAPbI3 interface, electron transfer, ETL free Perovskite solar cells, ultrafast dynamics.

In this work, we realize solar cells based on methylammonium lead iodide (MAPbI3) doped in solution with C70 fullerene in a mesoporous as well as in a planar electron transporting layer (ETL)-free architecture, showcasing in the latter case record efficiency of 15.7% and improved open circuit voltage (VOC). Contrarily to the bulk heterojunction previously reported, the C70 molecules do not phase segregate; rather, they are finely dispersed in the perovskite film, possibly infiltrating at the grain boundaries, while assisting the growth of a highly uniform perovskite layer. By means of time- resolved fs-to-ns optical spectroscopy, with an extended spectral coverage, we observe that electrons photogenerated in the perovskite are transferred to C70 with a time constant of 20 ps. Despite being captured by C70, electrons are not deeply trapped, and can potentially bounce back into the perovskite, as suggested by the high fill factor (FF) and enhanced VOC of the MAPbI3:C70 solar cells, especially in the case of the ETL-free device configuration.

Over the last decade, lead halide perovskite solar cells have been promoting a paradigm shift in the photovoltaic research, leading to device efficiencies of more than 23%[1–4]. Typical solar cells configuration consists of a multi-layered stack where the perovskite is sandwiched in between an electron transport layer (ETL),  usually TiO2, and an organic hole transporting material (HTM)[2,5,6]. Fullerenes and their derivatives have also been extensively used in perovskite solar cells as efficient electron extracting layer [7–9], however the fullerene/perovskite interaction is still subject of ongoing research [10,11]. Fullerenes have been shown to effectively passivate the mid-gap charge trap states in state-of-the art MAPbI3 solar cells, at both perovskite film surfaces and grain boundaries, partially infiltrating into the bulk. [12,13] This resulted in multiple beneficial actions such as reducing device hysteresis, [12,13]  blocking ion migration along the perovskite grain boundaries [13,14] as well as limiting the interfacial charge accumulation effect [14,15].  Nevertheless, a different proposed architecture consists in blending the fullerene with perovskite in a bulk-heterojunction like morphology [14,16,17] where fullerene intergranular layers are formed as charge percolation paths.  Improved conductivity has been demonstrated, related to the longer charge diffusion length and reduced recombination[14,17], and efficient electron transfer from perovskite to fullerene has been theoretically and experimentally validated, happening on the nanosecond time scale [18–20].

Differently from state of the art architectures [14], here we choose a different strategy by mixing the precursors of the MAPbI3 with C70-fullerene dispersion in solution. This results in a fine blend of the C70 molecules within the MAPbI3 matrix, avoiding the formation of a coarser phase separated morphology, as in the case of bulk heterojunctions. By using this approach, we developed mesoporous-TiO2, planar-TiO2 as well as ETL- free device configurations. A clear trend is observed: upon the doping with C70, the solar cell VOC increases independently from the device configuration. Remarkably, a simple planar, ETL-free MAPbI3:C70 cell processed by a low-temperature solution method delivers a record power conversion efficiency (PCE) of 15.7% with improved VOC = 1.065 V, surpassing the current records for such simple architecture [21–25]. We investigated the effects of the doping with C70 by monitoring the charge carrier dynamics over a broad time range from femtoseconds to nanoseconds combining transient absorption (TA) and photoluminescence (PL) measurements. Noteworthy, we investigate the ultrafast TA dynamics in an extended high photon energy spectral window, which has so far remained unexplored. We identify the signature of three conduction band-valence band transitions in the perovskite manifested as photobleaching (PB) bands which are quenched upon the addition of the C70 dispersion, suggesting that the photoinduced electrons in the perovskite are transferred to the C70. Although further work has to be done in order to fully understand the fate of the transferred electrons, the high device performances and VOC suggests that electrons are not deeply trapped in the C70 molecules but they can be transferred back to the perovskite, ensuring an efficient charge transport throughout the film, while possibly mitigating the charge trapping.

Perovskite solar cells are prepared by using a mixed solution of MAPbI3 (in dimethyl sulfoxide (DMSO), 1.25 M) and C70 (in o-xylene (2 mg/mL)), at 4:1 volume ratio. By controlling the deposition conditions, via one-step spin coating method (see SI for further details), a uniform perovskite film with comparable thickness for both planar and mesoporous configurations is obtained (see absorption spectra and scanning electro-microscopy (SEM) images in Figures S1-S2). Upon the addition of C70 dispersion, the absorption spectrum remains unaltered, due to the very small amount of C70 added (0.07 % in weight) (Figure 1a). Note that considering the density of perovskite and C70 (p=6.68 10-3 mol/cm3 and C70= 2.38 10-3 mol/cm3, respectively), such concentration implies 0.14% of volume occupied by the C70 with respect to MAPbI3. This prevents the formation of large C70 domains ensuring a proper dispersion within MAPbI3, possibly infiltrating at the crystal grain boundaries. Indeed, as observed in the SEM image (Figures 1 b-e), no evidence of coarse phase segregation is visible. On the other side, addition of C70 yields to a smoother morphology with a good film coverage (Figures 1 b-c, 1d-e and Figure S3). Such optimal coverage is particularly important for the ETL-free configuration in reducing the resistance shunting paths which usually limit the PCE of this architecture below 14% [24–26]. Furthermore, C70 assists the growth of highly crystalline films (see also X-ray diffraction pattern in Figure S4) with a reduced density of pinholes.

Figure 1f reports the steady-state PL spectra (dotted lines) of the MAPbI3 and MAPbI3:C70 samples upon excitation from the perovskite side, with the aim to interrogate the emissive properties of the perovskite bulk. For the latter, the PL signal of the film is quenched. While this measurement is not quantitative and does not reflect the entire mechanisms behind device operation, it indicates that a quenching process happens in presence of C70 molecules in the perovskite bulk. With the idea to shed light on the C70/perovskite dispersion, we examined the TA dynamics of the system. Figure 1a shows, on top of the PL spectra, the TA signal comparing MAPbI3 and MAPbI3:C70 integrated in the first 100 ns time frame upon exclusively exciting the MAPbI3 at 650 nm. A broad positive differential transmission (T/T) band peaking around 760 nm is observed, representing the PB signal due to charge state filling at the perovskite band edges [9,27,28]. Since the PB monitors the evolution of the charge populations, being proportional to the density of electrons and holes, the observed quenching suggests that a charge transfer process takes place to the C70 molecules, which can also account for the observed PL reduction. It is noteworthy that we excite with 50 nJ/cm2 fluence, corresponding to a photocarrier density of  1016 cm-3, an excitation regime in which traps are saturated and the intrinsic band-to-band electron-hole recombination dominates [29–32]. Thus, while in general the TA signal contains information on the total carrier population and its evolution mirrors both the radiative and non-radiative processes, in this case, we are in a fluence regime where traps are filled and the TA dynamics is mainly reflecting the radiative processes, hence, the time resolved PL and TA are expected to show the same dynamics, see Ref. 9. This allows for a fair comparison between PL and TA dynamics, as shown in Figure 1g. This does not implicate that, under device operation, the nonradiative channels are off, rather they are still a source of losses, as evident by the device Voc, limited to less than 1.1eV. For MAPbI3, the PL and the PB behaviors overlap with a mono-exponential decay fitted with a time constant of 1=110 ns, followed by a long living tail extending in the microsecond times (see Figure 1h). In agreement with the well-established rate equation model, assuming only single carrier trapping and band to band transitions to describe the PL decay [32], the faster decay reflects the band to band radiative transition, while the long living tail can be due to long-living trapped charges. Indeed, on longer timescale the PL decay slightly deviates from the ns TA and its lifetime increases (up to 2=600 ns) under weaker excitation of 4x1014 (see Figure 1h), for which the trapping process dominates. The films doped with C70, on the other hand, show a markedly different behavior. The PB signal decays with two time constants of 1=10 ns (close to the resolution limit of 8 ns), while reducing the amplitude of the long living tail (Figure 1 g) which decays with a time constant of 160 ns. Again, since we are at an excitation density were most of traps can be considered filled, [29-32] the second time constant can reflect the electron – hole recombination. It is worth noticing that this second time constant is slower in the blend with respect to the pure MAPbI3 (i.e. 110 ns), which might reflect, among other processes, that electron-hole recombination is slowed down in the blend upon electrons are bounced from the C70 molecules back to the perovskites. The PL follows the same behavior in the faster time window, indicating the opening of a new path for the escape of free charges. On longer time scale, a long-living signal possibly associated to shallow traps is visible, with an associated lifetime of 2=700 ns. This quenching effect can be associated to electron transfer to the C70 molecules. The decay at longer timescale (Figure 1h), on the other side, can provide information on the slower trap-mediated recombination processes. Comparing the long living tail, not much difference is observed when C70 is incorporated in the MAPbI3, enabling us to infer that the two materials possess a similar trapping rate and density. However, it is worth pointing out that a wide distribution of trap species exist in perovskites [33,34] and, more recently, shallow traps have been identified which get populated within 1 ns [29,35]. Thus, a possible effect of C70 on trap states cannot be entirely ruled out. Moreover, upon zooming out the PL decay in the first tens of ns (see Figure S5), a fast PL quenching is visible in presence of C70. Upon fitting the PL decay with a single-exponential function convoluted with a gaussian (which represents the response time of the instrument), the estimated PL lifetime for MAPbI3:C70 falls within 1ns, setting an upper limit for the electron transfer process, in agreement with established literature. [18]

To further understand the origin of the PB/PL quenching, we performed sub-picosecond TA by means of a narrowband pump combined with a broadband probe (generating white light from a CaF2 plate from 350 to 780 nm). Interestingly, there is only one report in literature [36] showing TA spectra in this high probe photon energy region. We excite the MAPbI3 slightly above the band gap using 650 nm pulse (duration 100fs) with a fluence of 4.7 μJ/cm2, corresponding to a charge density of around 1018 cm−3. Upon photoexcitation, three positive T/T features appear, peaking at 750 nm, 490 nm, and 410 nm (Figure 2a). The bands at 750 and at 490 nm have been already reported in literature and certainly assigned to the PB upon state filling of the perovskite conduction band (CB) and first and second valence band (VB), respectively, i.e. VB1CB1 and VB2CB1.[36–38] On the other hand, the band at 410 nm has been tentatively assigned in Ref. 39 both to a transition from valence band to a higher CB, such as VB2CB2 or to the transition from a lower VB to the CB, such as VB3CB1. [39] In our case, since the three bands show the same decay, not only in the case of the pristine MAPbI3, but also, more importantly, in the case of the MAPbI3/C70 where electron transfer happens from CB1 to the LUMO of the C70, we can conclude that this band is assigned to PB arising from the VB3CB1 transition as schematically depicted in Figure 2c. It is fair pointing out that, despite the semplicity of the cartoon showing the CB and VB as discrete levels, we are dealing with a semiconductor, thus it is more appropriate to speak about VB and CB rather than ground and excited states. The three PB bands, due to state filling of the CB and VB,  decay following a similar trend (see dynamics in Figure 2b), mirroring in the hundreds of ps the charge recombination paths, including charge trapping mechanisms [18,27,28,40,41]. Note that the high energy PB forms instantaneously after photoexcitation (within the 150-fs instrumental resolution) while the PB band at the band edge shows an additional rise completed in the first ps, following charge thermalization [42,43] (see Figure S6). Upon blending with C70, the position of the three PB bands remains unaltered, but the PB dynamics with C70 all show a faster decay, characterized by a time constant =20 ps. Considering the energy level alignment of the MAPbI3/C70 interface, this quenching is assigned to electron transfer to the C70 molecules. This is in agreement with recent works showing a favorable energetic alignement at the MAPbI3/fullerene for electron transfer [44, 45]. Interestingly, it has been found that efficient electron transfer happens only for few fullerene monolayers [44]. Above this limit, electron transfer is saturated and hampered. In our case, the blending of C70 within the solution ensures a fine dispersion of the C70 molecules and limits their aggregation, thus enabling an efficient electron transfer. Note that, considering a typical value for the electron diffusion coefficient in MAPbI3 of D  0.04 cm2/s [9], we can estimate that in the blend the electrons travels for an average distance LD=2Dτ 13 nm prior to the encounter with the C70 molecules where electron transfer happens (using =20 ps). Thus, the C70 molecules are well dispersed within the bulk of the perovskite, possibly infiltrating at the grain boundaries. This observation is further validated by measuring a planar interface consisting of 20 nm thick MAPbI3 layer interfaced with C70 evaporated on top (see data in Figure S7). In this case, the MAPbI3 PB gets quenched (see Figure S7) with a time constant = 40 ps. To further corroborate that the quenching is due to electron transfer we also analyzed the TA spectrum extended towards the IR region (data presented in Figure S8). Compared to pristine MAPbI3 showing a featureless positive signal which was previously ssigned to the PB of mid-gap trap states, [28] the bilayer shows the formation of a negative band beyons 1000 nm which is consistent with a photoinduced absorption (PA) band of the reduced C70 molecules. This further demonstrate that electron transfer to C70 happens upon charge diffusion in the perovskite film. The diffusion length, in this case, is ultimately dictated by the sample thickness of 20 nm.  Thus, we can estimate a diffusion constant of 0.05 cm2/s, in good agreement with what reported in the literature sofar and obtained for the finely dispersed morphology. In our case, the electron transfer to the C70 happens with a time constant of 20 ps, possibly preventing the electrons from getting trapped, while diffusing into the perovskite grain boundaries [12,44]. It is fair noticing that the LUMO of the fullerene has been most of the cases collocated rather close to the MAPbI3 conduction band [45]. This suggests the hyphotesis that, while electrons transferred to C70 in contact with the ETL can be efficiently collected, those captured by C70 dispersed in the perovskite bulk can bounce back to the perovskite, ensuring an efficient charge transport. Indeed, given the close energy match with the C70 LUMO and perovskite CB, 45 the electrons will not be deeply trapped and will easily escape, contributing in the device photocurrent. Indeed, as we will show below, it is importnat to notice that the devices doped with C70 outperform in terms of PCE and JSC, which would be incompatible with the transferred electrons being trapped in the C70, but fully consistent with a weak binding that allows back and forth exchange. To test the effect of C70 on photovoltaic performance, we fabricate a series of devices (Figure 3) using MAPbI3 with and without C70, considering three different architectures. With that aim, the perovskite is sandwiched in between the organic HTM on one side (spiro-OMeTAD), and either the mesoporous-TiO2 (meso-TiO2, Figure 3c), compact-TiO2 (c-TiO2, Figure 3b) or the conductive FTO glass (ETL-free configuration, Figure 3a), in the other side, following reported procedures[1,6]. We carefully control the deposition in order to produce films with similar thickness in all cases (see also the absorption spectra and SEM in Figures S1, S2). Noteworthy, the ETL-free device using MAPbI3:C70 blend exhibits an improved VOC =1.065 V (as compared to 1.045V without C70), comparable short-circuit current JSC =20.44 mAcm-2, and enhanced fill factor FF=0.72 (as compared to 0.67 without C70) resulting in an overall improved PCE of 15.7% (as compared to 14.65% without C70). See Table I for device parameters. The current-voltage (J-V) characteristics is reported in Figure 3d. To our knowledge, this is the highest value of PCE reported for an ETL-free perovskite device (device statistics is represented in Figure S8). A similar trend, i.e., an improvement of the VOC, is also observed for c-TiO2 or meso-TiO2 configurations, showing that the benefical effect of C70 is robust to device architectures. See the results from a Gaussian device statistics and the standard deviation of the mean, and the p value of a one-way ANOVA analysis reported for each case for the solar cell parameters (VOC, FF, JSC, PCE) in Figures S9-S12. Device parameters are listed in Table S1-S6. We ascribe this improvement to a double beneficial effect facilitated by the C70, assisting the growth of a more uniform perovskite morphology, as well as passivating electron traps. On the other side, irrespective of the presence of the TiO2 layer, the device photocurrent barely changes. This suggests that charge injection in the fullerene dispersion can reduce the electron scattering in the perovskite traps, overall improving the device VOC. Further details on device performance and measurement conditions, i.e. J-V characteristics in forward and back scan direction, are reported in Figure S13.

In conclusions, our study demonstrates the beneficial role of C70 fullerene incorporation into the MAPbI3 matrix even for very low relative amounts (below 0.05% M), where a bulk-heterojunction like morphology is not plausible to exist. By means of time-resolved PL and picosecond to nanosecond TA measurements, the electron transfer dynamics are highlighted. We demonstrate that, due to the favorable interface energy landscape, electrons are transferred from the perovskite to the C70 molecules on the picosecond time scale. With this strategy, using mixed MAPbI3:C70, we demonstrate PCE of 15.7%, with a short circuit current density of 20.44 mA/cm2, an open-circuit potential of 1.06 V and a fill factor of 0.72 for ETL-free cells, a record for this class of devices. Consequently, a direct impact on device performances as an enhancement of the solar cell open circuit voltage is observed, which manifests in both standard devices (using TiO2 as ETL) and, more interestingly, in ETL-free cells. We envisage that blending the MAPbI3 with a small amount of electron accepting molecules, forming a finely dispersed system, can open up a new way to reduce the trap density in the perovskite film. On the other side, being aware that both negatively and positively trapped charges coexist in the perovskite film, this blending procedure can be extended to organic hole accepting molecules, as a new route towards the development of trap-free perovskite films. In addition, our results suggest that the use of selective hole and electron transport layers may not be the ultimate approach to optimize charge transport and collection, while an optimized doped perovskite with an intermixed morphology can be an easier and preferential route for achieving low cost high-performance perovskite solar cells.

Experimental Section

Solar cell fabrication: Perovskite solar cells were fabricated on F-doped SnO2 (NSG10) substrates previously cleaned by a sequential sonication treatment in a 2 % Hellmanex solution, acetone and isopropanol, followed by UV ozone treatment for 15 min. A compact blocking layer of TiO2 (bl-TiO2, 30 nm in thickness) was then deposited onto the FTO glass substrate by spray pyrolysis, using a titanium diisopropoxide bis(acetylacetonate) solution in ethanol (60% v/v), and then sintered at 450 °C for 30 minutes. A 200-nm-thick layer of mesoporous TiO2 (meso-TiO2, 30 NR-D titania paste from Dyesol) was prepared by spin-coating a diluted TiO2 dispersion in ethanol, ratio 1:8 by weight, at 2000 rpm for 15s followed by a sintering step at 500 °C for 30 min. Afterwards, the substrates were lithium-treated by spin-coating 40 μl of tris(bis(trifluoromethylsulfonyl)imide) (Li-TFS ) (14.67mg/ml in acetonitrile) onto the mesoporous layer, followed by a sintering step at 500 °C for 30 min. The perovskite solution was prepared based on 1.25 M PbI2 /MAI (1:1) in dimethyl sulfoxide (DMSO). Besides, MAPbI3:C70 blends were prepared by adding 250 µl of a starting solution of C70 in o-xylene solvent (2 mg/ml) to 1000 µL of MAPbI3. The perovskite solution was then deposited by a two step spin coating method, starting at 1000 rpm for 10 s (500 rpm/s) and finalizing at 4000 rpm for 30 s (2000 rpm/s). 10s prior to the end, 100 µl of chlorobenzene were added onto the film to obtain a dense pinhole-free perovskite layer. Finally the films were annealed at 100 °C for 1h. After this time, spiro-OMeTAD was spin-coated at 4000rpm, 30s from a chlorobenzene solution (28.9mg in 400μl, 60m M) containing Li-TFSI (7.0μl from a 520 mg/ml stock solution in acetonitrile), TBP (11.5μl) and Co(II)TFSI (10 M%, 8.8μl from a 40 mg/ml stock solution) as dopants. Finally, a 70 nm gold electrode was evaporated.

Device Characterization.

The photovoltaic device performance was analyzed using a VeraSol LED solar simulator (Newport) producing 1 sun AM 1.5 (1000W/m2) sunlight. Current-voltage curves were measured in air with a potentiostat (Keithley 2604). The light intensity was calibrated with a NREL certified KG5 filtered Si reference diode. The solar cells were masked with a metal aperture of 0.16 cm2 to define the active area. The cells were measured in air, at room temperature and without encapsulation, at a constant rate 10 mV·s-1 for both forward and reverse bias. No special pre-conditioning protocol was used apart from 5 seconds of stabilization time before the measurement. No anti-reflective coating was used during the measurement.

Steady-state Optical Characterization. The absorption spectra were registered with an UV-VIS-IR spectrophotometer (PerkinElmer Instrument).

Time Resolved Photoluminescence: Photoluminescence (PL) Measurements: CW and time-resolved PL experiments were performed with a spectrophotometer (Gilden Photonics) using the lamp (at 650nm) or a pulsed source at 460 nm (Ps diode laser BDS-SM, pulse width < 100 ps, from Photonic Solutions, 20 MHz repetition rate, approx. 500 μm spot radius), respectively. The excitation fluence is around few nJ/cm2. The steady state spectra and the time-resolved signal were recorded by a photomultiplier tube and by a Time Correlated Single Photon Counting detection technique with a time resolution of 1 ns within a 40 ns time window. For extended time window the ns-TA system has been used to collect the emission.

ns-Transient Absorption Spectroscopy)/Photoluminescence: For ns-TA a ns laser (5ns pulse duration, 10Hz, Ekspla NT342 model) with an integrated optical parametric oscillator system (tunable from 355 to 2500nm) has been used as pump source. It is coupled with the LP980-KS Laser Flash Photolysis Spectrometer used for the measurement of laser induced TA, and PL kinetics and spectra. Wavelength specific kinetic measurements are made using photomultiplier and digital storage oscilloscope. The probe light is provided by a pulsed Xenon arc lamp. The beams are focused onto the sample on a diameter of minimum 5mm2 area, ensuring the spatial overlap. The transmitted probe is spectrally filtered by a monochromator and detected. From the transmission change following photoexcitation the variation in the absorption is thus derived as Δ(𝜏,𝜆)=log(𝐼𝑝𝑟𝑜𝑏𝑒)/(𝐼𝑡(𝜏,𝜆)), where Iprobe is the transmitted probe with excitation off and It is the transmitted probe after laser excitation. The minimum detectable optical density of the LP980-KS using the photomultiplier is OD = 0.002 (single shot, fast detector option) with a system overall response function of: <7ns (laser limited). For PL measurements the probe light was blocked and the emission upon pump excitation has been collected. Considering an excitation at 370 nm and a large spot size (r=0.03m) and a shorter penetration depth of around 100 nm, we retrieved for 50 nJ/cm2 a carrier density of ≈1016 carrier/cm3. All measurements were taken with the samples encapsulated with PMMA to prevent any effect from oxygen or sample degradation.

fs- Transient Absorption Spectroscopy: Our femtosecond TA spectrometer starts with an amplified Ti:sapphire laser, generating 4 mJ, 100 fs pulses at =800 nm and 1 kHz repetition rate. A 300 J fraction of the pulse energy was used for the experiments and split into two beams. The first beam fed an optical parametric amplifier (OPA), which generated tunable pump pulses in the visible region with about 70 fs duration; the second beam was focused in a transparent crystal, which generated a broadband white-light continuum (WLC) that spanned from 350nm to 780nm range and was used as a probe. A 3 mm thick CaF2 plate was used to generate the WLC in the visible region. Pump and probe pulses were non-collinearly focused on the sample and the transmitted probe, which was spatially selected by an iris, was

sent to a spectrometer (silicon for the visible range) capable of single-shot detection at the full 1 kHz repetition rate of the laser. The differential transmission (T/T) spectrum was obtained by recording the probe spectrum with and without the pump pulse. The pump beam energy density used in the experiment was deliberately kept low (pump fluence of

4.7 μJcm-2, which resulted in excitation densities in the order of 1018 cm-3, see Supporting Information for a detailed calculation of this value). All measurements were taken with the samples encapsulated with PMMA to prevent any effect from oxygen or sample degradation.

Supporting Information

Supporting Information is available from the Wiley Online Library or from the author.

Acknowledgements

We thank the European Commission H2020-SOLEDLIGHT project, grant agreement N°: 643791 for financial support. G.G. acknowledges the Swiss National Science Foundation (SNSF) funding through the Ambizione Energy project HYPER (grant number PZENP2_173641). G.C. acknowledges support by the European Union Horizon 2020 Programme under Grant Agreement No. 696656 Graphene Flagship. This work was partially supported by MINECO (Ministerio de Econom&a y Competitividad, Spain) under Grant Agreement MAT2013-47192-C3-2-R. The authors acknowledge Dr. Daniele Viola, Dr. Mariateresa Scarongella and Mr. Sadig Aghazada for usewful discussion.

Received: ((will be filled in by the editorial staff))
Revised: ((will be filled in by the editorial staff))
Published online: ((will be filled in by the editorial staff))

References

[1]	M. Saliba, T. Matsui, K. Domanski, J.-Y. Seo, A. Ummadisingu, S. M. Zakeeruddin, J.-P. Correa-Baena, W. R. Tress, A. Abate, A. Hagfeldt, M. Grätzel, Science 2016, 354, 206.

[2]	J.-P. Correa-Baena, A. Abate, M. Saliba, W. Tress, T. J. Jacobsson, M. Grätzel, A. Hagfeldt, Energy Environ. Sci. 2017, 10, 710-727 .

[3]	W. S. Yang, B.-W. Park, E. H. Jung, N. J. Jeon, Y. C. Kim, D. U. Lee, S. S. Shin, J. Seo, E. K. Kim, J. H. Noh, S. I. Seok, Science 2017, 356, 1376.

[4]	Http://www.nrel.gov/ncpv/images/efficiency_chart.jpg., n.d.

[5]	M. M. Lee, J. Teuscher, T. Miyasaka, T. N. Murakami, H. J. Snaith, Science 2012, 338, 643.

[6]	C. Roldan-Carmona, P. Gratia, I. Zimmermann, G. Grancini, P. Gao, M. Graetzel, M. K. Nazeeruddin, Energy Environ. Sci. 2015, 8, 3550.

[7]	Z. Zhu, J. Ma, Z. Wang, C. Mu, Z. Fan, L. Du, Y. Bai, L. Fan, H. Yan, D. L. Phillips, S. Yang, J. Am. Chem. Soc. 2014, 136, 3760.

[8]	K. T. Cho, G. Grancini, Y. Lee, D. Konios, S. Paek, E. Kymakis, M. K. Nazeeruddin, ChemSusChem 2016, 9, 3040.

[9]	S. D. Stranks, G. E. Eperon, G. Grancini, C. Menelaou, M. J. Alcocer, T. Leijtens, L. M. Herz, A. Petrozza, H. J. Snaith, Science 2013, 342, 341.

[10]	M. F. N. Taufique, S. M. Mortuza, S. Banerjee, J. Phys. Chem. C 2016, 120, 22426.

[11]	C. Quarti, F. De Angelis, D. Beljonne, Chem. Mater. 2017, 29 (3), 958–968.

[12]	Y. Shao, Z. Xiao, C. Bi, Y. Yuan, J. Huang, Nat. Commun. 2014, 5, 578.

[13]	J. Xu, A. Buin, A. H. Ip, W. Li, O. Voznyy, R. Comin, M. Yuan, S. Jeon, Z. Ning, J. J. McDowell, P. Kanjanaboos, J.-P. Sun, X. Lan, L. N. Quan, D. H. Kim, I. G. Hill, P. Maksymovych, E. H. Sargent, Nat. Commun. 2015, 6, 7081.

[14]	Y. Fang, C. Bi, D. Wang, J. Huang, ACS Energy Lett. 2017, 2, 782.

[15]	Z. Xiao, C. Bi, Y. Shao, Q. Dong, Q. Wang, Y. Yuan, C. Wang, Y. Gao, J. Huang, Energy Environ. Sci. 2014, 7, 2619.

[16]	C.-H. Chiang, C.-G. Wu, Nat. Photonics 2016, 10, 196.

[17]	K. Wang, C. Liu, P. Du, J. Zheng, X. Gong, Energy Environ. Sci. 2015, 8, 1245.

[18]	C. S. Ponseca, E. M. Hutter, P. Piatkowski, B. Cohen, T. Pascher, A. Douhal, A. Yartsev, V. Sundström, T. J. Savenije, J. Am. Chem. Soc. 2015, 137, 16043.

[19]	E. M. Hutter, J.-J. Hofman, M. L. Petrus, M. Moes, R. D. Abellón, P. Docampo, T. J. Savenije, Adv. Energy Mater. 2017, 7, 1602349.

[20]	   Z.    Zhu, Q. Xue, H. He, K. Jiang, Z. Hu, Y. Bai, T. Zhang, S. Xiao, K. Gundogdu, B. R. Gautam, H. Ade, F. Huang, K. S. Wong, H.-L. Yip, S. Yang, H. Yan, Adv. Sci. 2016, 3, 1500353

[21]	D. Liu, T. L. Kelly, Nat. Photonics 2014, 8, 133.

[22]	A. Mei, X. Li, L. Liu, Z. Ku, T. Liu, Y. Rong, M. Xu, M. Hu, J. Chen, Y. Yang, M. Grätzel, H. Han, Science 2014, 345, 295.

[23]	G. Grancini, C. Roldán-Carmona, I. Zimmermann, E. Mosconi, X. Lee, D. Martineau, S. Narbey, F. Oswald, F. D. Angelis, M. Graetzel, M. K. Nazeeruddin, Nat. Commun. 2017, 8, 15684.

[24]	R. Sandoval-Torrientes, J. Pascual, I. García-Benito, S. Collavini, I. Kosta, R. Tena-Zaera, N. Martín, J. L. Delgado, ChemSusChem 2017, 10, 2023.

[25]	D. Liu, J. Yang, T. L. Kelly, J. Am. Chem. Soc. 2014, 136, 17116.

[26]	J. Pascual, I. Kosta, T. Tuyen Ngo, A. Chuvilin, G. Cabanero, H. J. Grande, E. M. Barea, I. Mora-Seró, J. L. Delgado, R. Tena-Zaera, ChemSusChem 2016, 9, 2679.

[27]	G. Grancini, A. R. Srimath Kandada, J. M. Frost, A. J. Barker, M. De Bastiani, M. Gandini, S. Marras, G. Lanzani, A. Walsh, A. Petrozza, Nat. Photonics 2015, 9, 695.

[28]	G. Grancini, D. Viola, Y. Lee, M. Saliba, S. Paek, K. T. Cho, S. Orlandi, M. Cavazzini, F. Fungo, M. I. Hossain, A. Belaidi, N. Tabet, G. Pozzi, G. Cerullo, M. K. Nazeeruddin, ChemPhysChem 2017, 18 (17), 2381-2389

[29]	Y. Yamada, T. Yamada, A. Shimazaki, A. Wakamiya, Y. Kanemitsu, J. Phys. Chem. Lett. 2016, 7, 1972.

[30]	C. Wehrenfennig, M. Liu, H. J. Snaith, M. B. Johnston, L. M. Herz, Energy Environ. Sci. 2014, 7, 2269.

[31]	Y. Yamada, T. Nakamura, M. Endo, A. Wakamiya, Y. Kanemitsu, J. Am. Chem. Soc. 2014, 136, 11610.

[32]	S. D. Stranks, V. M. Burlakov, T. Leijtens, J. M. Ball, A. Goriely, H. J. Snaith, Phys. Rev. Appl. 2014, 2, 34007.

[33]	A. Baumann, S. Väth, P. Rieder, M. C. Heiber, K. Tvingstedt, V. Dyakonov, J. Phys. Chem. Lett. 2015, 6, 2350.

[34]	B. Kang, K. Biswas, Phys. Chem. Chem. Phys. 2017, 19, 27184.

[35]	A. R. Srimath Kandada, S. Neutzner, V. D’Innocenzo, F. Tassone, M. Gandini, Q. A. Akkerman, M. Prato, L. Manna, A. Petrozza, G. Lanzani, J. Am. Chem. Soc. 2016, 138, 13604.

[36]	A. Marchioro, J. Teuscher, D. Friedrich, M. Kunst, R. van de Krol, T. Moehl, M. Grätzel, J.-E. Moser, Nat. Photonics 2014, 8, 250.

[37]	L. Wang, C. McCleese, A. Kovalsky, Y. Zhao, C. Burda, J. Am. Chem. Soc. 2014, 136, 12205.

[38]	G. Xing, N. Mathews, S. Sun, S. S. Lim, Y. M. Lam, M. Grätzel, S. Mhaisalkar, T. C. Sum, Science 2013, 342, 344.

[39]	B. Anand, S. Sampat, E. O. Danilov, W. Peng, S. M. Rupich, Y. J. Chabal, Y. N. Gartstein, A. V. Malko, Phys. Rev. B 2016, 93, 161205.

[40]	X. Wu, M. T. Trinh, D. Niesner, H. Zhu, Z. Norman, J. S. Owen, O. Yaffe, B. J. Kudisch, X.-Y. Zhu, J. Am. Chem. Soc. 2015, 137, 2089.

[41]	C. S. Ponseca, T. J. Savenije, M. Abdellah, K. Zheng, A. Yartsev, T. Pascher, T. Harlang, P. Chabera, T. Pullerits, A. Stepanov, J.-P. Wolf, V. Sundström, J. Am. Chem. Soc. 2014, 136, 5189.

[42]	P. Piatkowski, B. Cohen, F. J. Ramos, M. D. Nunzio, M. K. Nazeeruddin, M. Grätzel, S. Ahmad, A. Douhal, Phys. Chem. Chem. Phys. 2015, 17, 14674.

[43]	J. M. Richter, F. Branchi, F. V. de A. Camargo, B. Zhao, R. H. Friend, G. Cerullo, F. Deschler, Nat. Commun. 2017, 8, 376.

[44]	C. Wang, C. Wang, X. Liu, J. Kauppi, Y. Shao, Z. Xiao, C. Bi, J. Huang, Y. Gao, Appl. Phys. Lett. 2015, 106, 111603.

[45]	S. Olthof, APL Mater. 2016, 4, 91502.

Figures

Figure 1. a. Absorption Spectra of the MAPbI3 and MAPbI3:C70 films deposited on compact TiO2 (c-TiO2) and encapsulated with PMMA. b, c. cross-section scanning electron microscopy (SEM) images and d, e. top SEM images for MAPbI3 and MAPbI3:C70, respectively. f. Integrated TA Spectra (filled symbols) and CW-PL spectra (open symbols) for the MAPbI3 and MAPbI3:C70 films deposited on compact glass substrate and encapsulated with PMMA. A fluence of 50 nJ/cm2 corresponding to a photocarrier density of around 1016 cm-3 is used for the ns-TA. g. ns-TA decay at 760 nm probe wavelength and PL decay registered at 780 nm for the MAPbI3 and MaPbI3:C70 films deposited on compact glass substrate and encapsulated with PMMA. h. PL decay comparing photocarrier density of around 3x1016 cm-3 to 4x1014 cm-3 upon excitation at 370 nm for MAPbI3:C70 (left panel) and MAPbI3 (right panel) deposited on compact glass substrate and encapsulated with PMMA.

Figure 2. a, d. Differential Transmission (T/T) spectra for MAPbI3 and MAPbI3:C70 films deposited on fused silica upon excitation at 650 nm with a fluence of 4.7 μJ/cm2 corresponding to ≈ 1018 carrier/cm3, respectively. b, e. T/T (dynamics at selected probe wavelengths as indicated in the legend, corresponding to the three main PB bands as indicated by the arrows in Figure 2 a,d. c, f.  Cartoon of the energy diagram scheme for the MAPbI3 and MAPbI3:C70, respectively deposited on compact glass substrate and encapsulated with PMMA.

Figure 3. a, b, c. Device schemes and d, e, f. current- voltage (J-V) characteristics comparing the devices using MAPbI3 with and without the C70 blend in three different architectures where the perovskite is deposited  directly on the conductive FTO glass, in a ETL-free configuration, on compact-TiO2 or infiltrated in the mesoporous-TiO2 scaffold.

Table 1. Device parameters (JSC, Voc, FF, PCE) for the devices reported in Figures 3 d, e, f)

| Sample | Jsc [mAcm-2] | Voc [V] | FF | PCE [%] |
| --- | --- | --- | --- | --- |
| FTO/MAPbI3 | 20.64 | 1.046 | 0.67 | 14.65 |
| FTO/MAPbI3:C70 | 20.44 | 1.065 | 0.72 | 15.71 |
| FTO/c-TiO2/ MAPbI3 | 21.45 | 1.05 | 0.71 | 16.17 |
| FTO/c-TiO2/ MAPbI3:C70 | 21.79 | 1.071 | 0.73 | 17.10 |
| FTO/c-TiO2/ TiO2/MAPbI3 | 21.87 | 1.07 | 0.78 | 18.34 |
| FTO/c-TiO2/ TiO2/MAPbI3:C70 | 22.33 | 1.079 | 0.79 | 19.19 |

Copyright WILEY-VCH Verlag GmbH & Co. KGaA, 69469 Weinheim, Germany, 2016.