Reversion of P-gp-mediated Drug Resistance in Ovarian Carcinoma Cells with PHPMA-Zosuquidar Conjugates

Claudia Battistella and Harm-Anton Klok*

École Polytechnique Fédérale de Lausanne (EPFL), Institut des Matériaux et Institut des Sciences et Ingénierie Chimiques, Laboratoire des Polymères, Bâtiment MXD, Station 12, CH-1015 Lausanne, Switzerland.

AUTHOR EMAIL ADDRESSES claudia.battistella@epfl.ch, harm-anton.klok@epfl.ch

CORRESPONDING AUTHOR FOOTNOTE harm-anton.klok@epfl.ch,  Tel: + 41 21 693 4866

ABSTRACT

Inhibition of P-glycoprotein (P-gp) transporter is an attractive approach for the reversion of cancer-associated multidrug resistance (MDR). PHPMA-based carriers that are able to release the anticancer drug doxorubicin in the lysosomes have shown promise to reduce P-gp mediated resistance. This is attributed to the release of the drug in close proximity to the nucleus and distant from the P-gp transporter. This work presents a strategy to maximize P-gp inhibition and enhance doxorubicin cytotoxicity in cancer cells by using a dual functional PHPMA conjugate carrying both the anticancer drug doxorubicin and the P-glycoprotein inhibitor zosuquidar (Zos). While doxorubicin was connected to the polymer backbone via a lysosomally cleavable spacer, the P-gp inhibitor Zos was attached by a hydrazone linker in order to promote release in the early stage of the endocytic process and maximize its cytosolic concentration in proximity of the P-gp transporter. Following Zos modification and determination of its ability to inhibit P-gp, conjugation to the PHPMA polymer backbone resulted in enhanced doxorubicin cytotoxicity in resistant A2780ADR ovarian carcinoma cells. Finally, the incorporation of both Dox and Zos in a single polymer carrier enhanced P-gp inhibition as compared to a control PHPMA conjugate containing only Dox.

INTRODUCTION

Chemotherapeutic agents are widely used to combat cancer. The onset of intrinsic or acquired multidrug resistance (MDR), however, a phenomenon in which cancer cells become resistant to an array of structurally and functionally unrelated chemotherapeutic agents, can lead to a poor clinical outcome.1 For instance, over 90% of the metastatic cancers do not respond to chemotherapy due to resistance mechanisms resulting in therapy failure.2 One of the most common mechanisms that can lead to the resistance of cancer cells to chemotherapeutics is associated with the presence of membrane transporter proteins, which are overexpressed on cancer cells.3-8 P-glycoprotein (P-gp), in particular, acts as an efflux pump that can decrease the intracellular concentration of chemotherapeutics. Doxorubicin, daunorubicin, vincristine, vinblastine, paclitaxel, docetaxel and bisantrene are examples of widely used anticancer drugs that are also P-gp substrates.1, 3, 9 The occurrence of P-gp mediated cross-resistance requires the use of higher dosages of these anticancer drugs, which further aggravates the survival rate of the patients due to the onset of numerous and intolerable side effects.10

A number of approaches have been developed to combat P-gp mediated MDR. A first strategy is the use of low molecular weight P-gp inhibitors.3 The first two generations of these P-gp inhibitors, however, were hampered by relatively low binding affinities and selectivities requiring high dosages and resulting in unacceptable in vivo toxicity.3, 10, 11 These issues could be partially resolved by a third generation of P-gp inhibitors, which were characterized by a higher specificity and affinity towards the P-gp transporter and lower toxicity.3 In spite of these refinements, the co-administration of low molecular weight P-gp inhibitors and chemotherapeutics still suffers some limitations. First, there is the unpredictable pharmacokinetics of the two unrelated drugs, which may lead to different time scales for their accumulation in the target cells.10-13 A second problem is the lack of selectivity of small molecule drugs towards cancer tissues, which causes an undesirable accumulation of these drugs also in healthy cells.11, 12, 14 It is important to mention that P-gp is not only expressed in cancer cells, but also in healthy tissues where this transporter protein plays a central role in the detoxification and protection of the organism against xenobiotics.1, 3, 11 Hence, the incapability of the P-gp inhibitors to distinguish between healthy and cancer tissues can enhance the distribution of the anticancer drugs in healthy cells and therefore further increase the chemotherapy-associated side effects.

A second promising avenue to address MDR exploits concepts from nanomedicine to co-deliver chemotherapeutics and P-gp inhibitors. Co-administration of a chemotherapeutic and a P-gp inhibitor with a single nanoparticle carrier or in the form of a single polymer conjugate offers a number of potential benefits. A first consequence of the co-delivery of the two active compounds with a single nanoparticle or a single polymer carrier is that the pharmacokinetics will be governed by that of the nanoparticle or polymer carrier. The use of nanoparticles or polymer carriers also allows to exploit active or passive (enhanced permeation and retention (EPR) effect) targeting strategies that can enhance delivery to cancer cells and reduce off-target delivery.15 Also on the cellular level the use of nanoparticles or polymer conjugates to co-deliver P-gp inhibitors and chemotherapeutics offers advantages. Macromolecules and nanoparticles are usually internalized by cells via endocytosis.16-18 This process involves the compartmentalization of nanoparticles and polymers in the endosomes and lysosomes, which generates a barrier that prevents rapid efflux and also allows to release the payload deeper inside the cell and in closer proximity of the respective target (and as a consequence more distant from the membrane-bound P-gp transporter).19, 20 This is particularly attractive for cancer therapy since a number of chemotherapeutics act on targets located in the nucleus. A number of reports have described the use of polymer or nanoparticle-based delivery strategies to combat MDR.12, 14, 19-22 Minko et al. investigated the effect of N-(2-hydroxypropyl) methacrylamide (PHPMA) copolymers that carried doxorubicin (Dox) attached via the lysosomally cleavable GFLG peptide linker on the viability of A2780 sensitive and A2780ADR multidrug resistant human ovarian cancer cells.19 These experiments indicated that while the IC50 value for the free Dox was 38 times larger on the A2780ADR resistant cells as compared to the sensitive cells, the difference between the two IC50 values was only about 20% for the polymer-Dox conjugate. The smaller difference in IC50 value between the resistant and sensitive cells that was observed for the polymer conjugate was attributed to the lysosomal release of Dox in close proximity to the target and distant from the P-gp efflux transporter.19 Moreover, chronic exposure of the sensitive cells to the polymer conjugate did not induce acquired MDR.20 More recently, Subr et al. investigated the cytotoxicity of a series of PHPMA conjugates that were modified with a peptide-based P-gp inhibitor and Dox via a pH-sensitive hydrazone linker.22 Whereas the hydrazone-linked Dox-PHPMA conjugate did not show any cytotoxicity towards MDR cells, copolymers that incorporated both the P-gp inhibitor and Dox as well as co-administration of Dox- and P-gp inhibitor-conjugates proved effective towards MDR cells.

The findings summarized above indicate that spatiotemporal release of Dox is important to evade efflux in MDR cells. This is illustrated by the fact that lysosomal release of Dox has been found to lead to a reduction of its efflux,19 whereas the use of the pH-sensitive hydrazone linker, which releases Dox earlier in the endocytic pathway in the endosomes, did have no effect in reducing P-gp mediated resistance.22 On the other hand, the results obtained with the hydrazone linked Dox-PHPMA copolymer also indicate that the pH-induced release in the early endosomes provides a relatively rapid pathway to the P-gp membrane transporter.22 In this study we attempt to capitalize on these findings and report (dual functional) PHPMA conjugates that allow spatially controlled release of the anticancer drug Dox and the third generation P-gp inhibitor zosuquidar (Zos).3, 23 The PHPMA conjugates presented here are not only able to simultaneously transport Zos and Dox into the cancer cells, but also exploit differences in the physicochemical environment in the endosomal and lysosomal compartments to release Zos and Dox by cleavage of two orthogonal linkers. Zos was attached via a pH-sensitive hydrazone linker designed for cleavage in the endosomes,24, 25 whereas Dox was conjugated via the lysosomally degradable GFLG peptide linker.19 The first part of this work investigates the feasibility of using PHPMA conjugates bearing a pendant Zos derivative via a hydrazone linker to overcome Dox efflux in resistant ovarian cancer cells. The second part describes a dual delivery system in which both drugs are conjugated to the PHPMA backbone via orthogonal cleavable linkers.

EXPERIMENTAL SECTION

MATERIALS

# 4-Acetylbenzoic acid, 2,2′-azobis(2-methylpropionitrile) (AIBN), 4,4′-azobis(4-cyanovaleric acid), 1-amino-2-propanol (HPA), 4-cyano-4-(phenylcarbonothioylthio)pentanoic acid (CTA), cysteamine hydrochloride, N-(3-dimethylaminopropyl)-N′-ethylcarbodiimide hydrochloride (EDC HCl), N,N′-dicyclohexylcarbodiimide (DCC), 2,2′-dipyridyl disulphide, 4-(dimethylamino)pyridine (DMAP), isobutyl chloroformate, 2,6-lutidine, 3-(4,5-dimethylthiazol-2-yl)-2,5-diphenyltetrazolium bromide) (MTT), 6-maleimidocaproic acid, methacryloyl chloride, N-methylmorpholine, tert-butyl carbazate and tris(2-carboxyethyl)phosphine hydrochloride (TCEP) were obtained from Sigma Aldrich. TECP was neutralized prior use by treatment with 0.1 N NaOH (until pH 6.5 was achieved) and sebsequently lyophilized. The neutralized TCEP was then dissolved in dry methanol, filtered and dried under vacuum. Pentafluorophenol was purchased from MatrixScientific, 3,3,3-trifluoropropylamine hydrochloride was obtained from Apollo Scientific and 3,3'-diethyloxacarbocyanine iodide (DiOC2(3)) from Life Technologies.  Fmoc-protected amino acids and Fmoc-Gly-Wang resin (100-200 mesh, loading 0.60 mmol/g) were obtained from Novabiochem. Ethyl(hydroxyimino)cyanoacetate (OxymaPure) and N,N,N′,N′-tetramethyl-O-(1H-benzotriazol-1-yl)uronium hexafluorophosphate (HBTU) were purchased from IRIS Biotech. Doxorubicin hydrochloride (Dox) was purchased from ShangHai Biochempartner and zosuquidar trihydrochloride (Zos) was obtained from NCE Biomedical. Diisopropylethylamine (DIPEA), triisopropylsilane (TIS), piperidine, dimethylformamide (DMF), dimethyl sulfoxide (DMSO), N-methylpyrrolidone (NMP) and trifluoroacetic acid (TFA) were obtained from VWR. Dichloromethane (DCM), tetrahydrofuran (THF) and diethylether were purchased from Reactolab and methanol (MeOH) from Merck. MeOH, DMF and THF were dried using a Pure Solv solvent purification system prior use. Triethylamine (Et3N) and 1,4-dioxane were purchased from Acros Organics. 1,4-Dioxane was dried over molecular sieves and Et3N was freshly distilled prior use. Pentafluorophenyl methacrylate (PFMA) was synthesized as reported by Eberhardt et al.26 The synthesis of the fluorinated CTA (F3-CTA), 2-(pyridyldithio)-ethylamine (PDA) and 6-maleimidocaproic acid hydrazide trifluoroacetic salt is described in the Supporting Information.

METHODS

NMR spectroscopy. 1H-, 19F- and 13C-NMR spectra were recorded on a Bruker AV-400 instrument at room temperature. 1H-NMR analysis of polymer conjugates was performed with a relaxation time (d1) of 10 seconds and at least 256 scans using CD3OD, CDCl3 or D2O as solvent. Chemical shifts are reported relative to the residual proton signal of the solvent.

Size exclusion chromatography (SEC). Size exclusion chromatography (SEC) of PPFMA was performed using an Agilent 1260 infinity system equipped with a Varian 390-LC refractive index detector, two PLgel 5 m Mixed C (Agilent) columns and a PLgel guard column. THF was used as eluent with a flow rate of 1 mL/min and the temperature was 40 °C. Samples were analysed using conventional calibration with polystyrene (PS) standards ranging from 4910 Da to 549 KDa. PHPMA conjugates were analysed with a Waters Alliance GPCV 2000 system. The eluent was DMF containing 0.01 wt % LiCl at a flow rate of 0.6 mL/min at 60 °C. The system was equipped with a refractive index detector and samples were analysed using conventional calibration with poly(methyl methacrylate) (PMMA) standards ranging from 3670 Da to 520 KDa.

UV-Vis spectroscopy. The mol % of Dox and 2-(pyridyldithio)-ethylamine (PDA) incorporated in the conjugates as well as the pH dependent release of Zos-Ket from the conjugates were determined using a Varian Cary 100 Bio spectrometer using quartz cuvettes.

Flow cytometry. Flow cytometry was performed using a BD Accuri C6 cytometer (BD Biosciences) equipped with a blue (488 nm) and red (640 nm) laser and the data were analysed using FlowJo software.

PROCEDURES

Synthesis of Zos-Ket (Scheme S4). 300 mg Zos (0.47 mmol) were dissolved in 8 mL chloroform and stirred with 3.3 equiv. (218 L) triethylamine (Et3N) for 15 minutes. The organic phase was washed twice with water, dried over MgSO4, filtered and finally dried under vacuum to yield zosuquidar free base. Next, 120 mg 4-acetylbenzoic acid (0.73 mmol), 1.1 equiv. (206.3 mg) DCC and 0.2 equiv. (18 mg) DMAP were dissolved in 7 mL dry DCM. 215 mg (0.41 mmol) zosuquidar free base were dissolved in 4 mL dry DCM and subsequently added to the active ester solution. The reaction was stirred under nitrogen at room temperature for 18 h. Following the reaction, the formed N,N'-dicyclohexylurea was removed by filtration and the crude product was purified by flash chromatography using ethyl acetate/hexane (6.5:3.5) to give the pure Zos-Ket (79 % yield). 1H-NMR, 19F-NMR and mass spectra are included in Figure S7 - S9.

Synthesis of Zos-Mal (Scheme S5). Zos-Mal was prepared according to a literature procedure with some small modifications.25 Briefly, 27 mg Zos-Ket (0.04 mmol) and 3 equiv. (41 mg) 6-maleimidocaproic acid hydrazide trifluoroacetic acid salt were dissolved in 2 mL dry methanol and stirred at room temperature for 1.5 h. The solvent was removed under reduced pressure and the residue was purified by preparative TLC using chloroform/methanol (10:0.3) as eluent to yield Zos-Mal (60 % yield). 1H-NMR, 19F-NMR and mass spectra are included in Figure S10 - S12.

Synthesis of Fmoc-GFLG-OH. Fmoc-GFLG-OH was synthesized on a CEM Liberty automated microwave synthesizer using Fmoc-Gly-Wang resin (0.5 mmol scale) and Fmoc chemistry without final Fmoc-deprotection.27 The peptide was purified by reversed phase high performance liquid chromatography (RP-HPLC) using a Shimadzu LC-20A Prominence preparative HPLC system equipped with a Vydac 218TP column (22 x 150 mm) that was operated at a flow rate of 20 mL/min. Peptide purification was achieved using two mobile phases. Mobile phase A consisted of a 0.05 % (v/v) solution of TFA in MilliQ water and mobile phase B consisted of a 0.05 % (v/v) solution of TFA in acetonitrile. The peptide was purified using a linear AB gradient from 35 % (v/v) to 55 % (v/v) of B over a period of 45 min and subsequently characterized via RP-HPLC-MS using a Vydac 218TP column (4.6x150 mm). The HPLC chromatogram and ESI mass spectrum of the peptide are shown in Figure S13.

Synthesis of NH2-GFLG-Dox (Scheme S6). 200 mg Fmoc-GFLG-OH (0.32 mmol) and 1.2 equiv. Dox (226.3 mg) were dissolved in 8 mL dry DMF. Next, 2 equiv. (136 L) DIPEA were added and the solution was stirred under nitrogen in the dark for 15 minutes. Then, 1.1 equiv. (162.7 mg) HBTU was dissolved in 1 mL dry DMF and subsequently added to the solution. The reaction mixture was stirred under nitrogen in the dark for three hours. Following the reaction, DCM was added to the solution and the organic phase was washed with 10 % acetic acid in water, passed over MgSO4, filtered and dried under vacuum to yield 320 mg Fmoc-GFLG-Dox that was used without further purification. Fmoc-deprotection was performed as follows: 100 mg Fmoc-GFLG-Dox (0.086 mmol) were dissolved in 400 L 10 % piperidine in DMF and the reaction was stirred for 5 minutes at 0 °C. 0.5 mL 0.5 M formic acid solution in DMF was added dropwise until the reaction color turned from blue to red. Next, the product was immediately precipitated in ice-cold diethyl ether. The recovered product was resuspended in fresh diethyl ether, centrifuged 2 times and finally purified by RP-HPLC using a linear AB gradient from 30 % (v/v) to 45 % (v/v) of B over a period of 30 min (yield 86 %). The purity, higher than 99 %, was determined by RP-HPLC-MS. The HPLC chromatogram and ESI mass spectrum of NH2-GFLG-Dox are shown in Figure S14. The 1H-NMR spectrum is reported in Figure S15.

Synthesis of PPFMA-1 and PPFMA-2. Two different PPFMA precursors, PPFMA-1 and PPFMA-2, were used for the synthesis of the PHPMA conjugates. The synthesis of these polymers is outlined in Scheme S7 and described in detail in the Supporting Information. The targeted molecular weight was around 20000 g/mol.19 Figure S16A shows a 19F-NMR spectrum of PPFMA-2. Figure S16B and Figure S16C show SEC plots of the two polymers. Detailed characteristics of PPFMA-1 and PPFMA-2 are summarized in Table S1.

Synthesis of PHPMA-PDA-1 and PHPMA-PDA-2. PHPMA-PDA-1 was obtained via post-polymerization modification of PPFMA-1, whereas PHPMA-PDA-2 was prepared from PPFMA-2. For the synthesis of PHPMA-PDA-1, 800 mg PPFMA-1 (3.2 mmol of PFMA reactive units) were dissolved in 10 mL dry DMF and 0.3 equiv. PDA (202.2 mg), 1.7 equiv. (417 L) 1-amino-2-propanol (HPA) and 2 equiv. (886 L) Et3N were added. For PHPMA-PDA-2, 800 mg PPFMA-2 were dissolved in 10 mL dry DMF and 0.4 equiv. PDA (282.9 mg), 1.6 equiv. (392 L) 1-amino-2-propanol (HPA) and 2 equiv. (886 L) Et3N were added. The solutions were stirred under nitrogen at 50 °C for 20 hours. The products were isolated by three precipitations in ice-cold diethyl ether and subsequently dialyzed against water/methanol for 2 days using a SpectraPor (MWCO 3.5 KDa) membrane and finally lyophilized. The mol % of PDA moieties incorporated in PHPMA-PDA-1 and PHPMA-PDA-2 were determined by UV-Vis and 1H-NMR spectroscopy and are summarized in Table S2. Details on the UV-Vis protocol are provided in the Supporting Information together with the UV-Vis, 1H-NMR spectra and SEC plots (Figure S17 - S20).

Synthesis of PHPMA-Dox-PDA. 60 mg PPFMA-2 (0.24 mmol of PFMA units) were dissolved in 3 mL dry DMF together with 0.15 equiv. (32.8 mg) NH2-GFLG-Dox and 0.2 equiv. (7 L) Et3N. The solution was stirred under nitrogen at 40 °C for 24 hours in the dark. After 24 hours, 1 mL DMF solution containing 0.1 equiv. (5.3 mg) PDA, 1.9 equiv. (35 L) HPA and 2 equiv. (66 L) Et3N was added and the reaction was stirred for an additional 20 hours at 40 °C. The product was precipitated three times in ice-cold diethyl ether, dialyzed against water/methanol for 2 days using a SpectraPor (MWCO 3.5 KDa) membrane and finally lyophilized. The mol % of PDA and Dox moieties incorporated in the conjugates conjugates were determined by UV-Vis and NMR spectroscopy and are indicated in Table S2. The UV-Vis procedure is provided in the Supporting Information together with the corresponding UV-Vis spectra (Figure S18). A 1H-NMR spectrum of PHPMA-Dox-PDA is included in Figure S21.

Synthesis of PHPMA-Dox. 100 mg PPFMA-2 (0.4 mmol of PFMA units), 0.2 equiv. (72 mg) NH2-GFLG-Dox and 0.2 equiv. (11 L) Et3N were dissolved in 4 mL dry DMF and stirred in the dark at 50 °C for 20 hours under nitrogen. After 24 h, 1 mL DMF containing 2 equiv. (60 L) HPA and 2 equiv. (110 L) Et3N was added and the reaction was stirred at 50 °C for an additional 20 hours. Following three precipitations from ice-cold diethyl ether, the product was dialyzed against water/methanol for 2 days using a SpectraPor (MWCO 3500 g/mol) membrane and finally lyophilized. The Dox content in the polymer conjugate was determined by UV-Vis and 1H-NMR spectroscopy. The corresponding UV-Vis and 1H-NMR spectra are included in Figure S18 and Figure S22 and the Dox content is listed in Table S2.

Synthesis of PHPMA-Zos-1 and -2 and PHPMA-Dox-Zos conjugates. PHPMA-Zos-1 and -2 and PHPMA-Dox-Zos conjugates were prepared by reacting the corresponding precursors (PHPMA-PDA-1, -2 and PHPMA-Dox-PDA) with an excess of Zos-Mal. A general procedure is as follows: 30 mg of the appropriate precursor polymer were dissolved in 4 mL dry methanol together with 3 equiv. (with respect to the PDA) freshly prepared Zos-Mal. After that, 3 equiv. neutralized TCEP were added dropwise and the solution stirred under nitrogen at room temperature overnight. The products were recovered by three precipitations from ice-cold diethyl ether and dialyzed with a SpectraPor dialysis membrane (MWCO 3.5 KDa) against PBS for 5 h and against water/methanol overnight and finally lyophilized. The Zos content of the polymer conjugates was determined by NMR spectroscopy and are listed in Table 1 and Table S2. 1H-NMR spectra of PHPMA-Zos-1, PHPMA-Zos-2 and PHPMA-Dox-Zos as well as 19F-NMR spectra of PHPMA-Zos-2 and PHPMA-Dox-Zos are included in Figure S23 - S27.

pH Triggered release of Zos-Ket from the PHPMA-Zos-1 conjugate. Zos-Ket release from PHPMA-Zos-1 was determined with a dialysis experiment by incubating the polymer conjugate in 0.1 M phosphate citrate buffer at pH 7.4 and 5.5 at 37 °C. Briefly, 2.7 mg polymer were dissolved in 200 L of each buffer solution and placed in SpectraPor micro dialysis cassettes with a molecular weight cut-off of 3.5 KDa. The samples were dialyzed against 2 mL of the same buffer solution. 30 % ethanol was added to all the buffers in order to assure complete dissolution of the cleaved Zos-Ket at the tested concentrations. Over a period of 40 hours at different time intervals, 300 L aliquots were taken and replaced with an equivalent amount of buffer. The aliquots taken from the dialysis cassettes were diluted to 600 L and the Zos-Ket content determined by UV-Vis spectroscopy by measuring the absorbance at  = 240 nm using cuvettes with a optical path of 0.1 cm. The Zos-Ket concentration was calculated using the molar extinction coefficients  = 26768 M-1 cm-1 and   = 25313 M-1 cm-1 ( = 240 nm) in the buffer solutions at pH 7.4 and 5.5, respectively. The corresponding calibration curves are shown in Figure S28.

Cell lines and cell cultures. The human ovarian carcinoma sensitive A2780 and resistant A2780ADR cell lines were kindly provided by Prof. S. O. Kelley, University of Toronto. Cells were cultured in RPMI 1640 glutamax (Lifetech) medium supplemented with 10 % fetal bovine serum (FBS) (Gibco) and 1% penicillin/streptomycin (Lifetech). A2780ADR cells were grown in media containing 200 nM doxorubicin in order to maintain the MDR-phenotype, 24 h before each experiment the medium was exchanged with fresh doxorubicin-free culture medium. Both cell lines were maintained in a humidified atmosphere containing 5 % (v/v) CO2 at 37 °C.

Cytotoxicity assay. Cytotoxicities were assessed using the MTT assay. To this end, 100 μL cell suspension, corresponding to 5000 A2780ADR and 2500 A2780 cells, were added to a 96-well flat bottom plate and subsequently pre-incubated for 24 h in complete growing medium. Then, 100 μL of a solution containing the compounds to be evaluated was added and the plates were incubated for another 72 h. Subsequently, the medium was aspirated and 110 μL of MTT solution (0.5 mg/mL) in medium without phenol red was added to each well and the plates incubated for an additional 3 h. After that, the medium was removed and 100 μL DMSO was added to each well to dissolve the purple formazan crystals formed by the mitochondrial dehydrogenase activity of viable cells. Plates were incubated at 37 °C for 15 minutes and the optical density was quantified spectroscopically using a TECAN infinite 200 PRO plate reader. The optical density, directly proportional to the number of viable cells, was quantified at 570 nm using a reference filter at 690 nm. The absorbance of wells without cells was used as background and cell viabilities were calculated as a percentage relative to untreated cells. All the results are means from at least two independent experiments, each comprising triplicates per drug concentration. IC50 values (concentration of drug necessary to inhibit 50 % of the cells growth) and standard errors were calculated using a sigmoidal dose-response curve fitting.

3,3'-Diethyloxacarbocyanine iodide (DiOC2(3)) efflux assay. Cells were trypsinized and resuspended in RPMI 1640 medium without antibiotics at a density of 1 × 106 cells/mL and transferred into different tubes. Cells were then incubated with varying concentrations of the appropriate P-gp inhibitor (Zos, Zos-Ket) or Zos-polymer conjugate (PHPMA-Zos-1, PHPMA-Zos-2) as well as with 20 M of the positive control cyclosporine A (CsA) for 3 h at 37 °C. After 20 minutes exposure to 1 g/mL DiOC2(3) solution in ice, cells were washed and incubated at 37 °C with and without the tested compounds for an additional 90 minutes. Cells were washed twice with fresh medium, suspended in 500 L of ice-cold medium and analysed by flow cytometry using the FL 1 channel for DiOC2(3) detection. Each experiment was repeated at least twice and results are reported as relative fluorescence, which represents the ratio between the geometric mean fluorescence of each sample and the positive control CsA.

Doxorubicin efflux assay. Cells were trypsinized and resuspended in RPMI 1640 medium without antibiotics at a density of 1 × 106 cells/mL and transferred into different tubes. Cells were then incubated with RPMI 1640 medium without antibiotics containing 10 M of free doxorubicin or doxorubicin-polymer conjugate either alone or in combination with 20 M of CsA for 4 h at 37 °C. Cells were washed twice with fresh medium, suspended in 500 L of ice-cold medium and analysed by flow cytometry (Dox was detected in the FL 2 channel). Each experiment was repeated at least twice and results are reported as relative fluorescence that represents the ratio between the geometric mean fluorescence of each sample and the samples containing the same tested compounds and CsA.

RESULTS AND DISCUSSION

PHPMA conjugate design and synthesis

The structure and synthesis of the PHPMA conjugates investigated in this study are shown in Scheme 1. In addition to the dual function PHPMA conjugate that was designed to co-deliver Dox and Zos (PHPMA-Dox-Zos) also monofunctional conjugates, which present either Zos (PHPMA-Zos-1 and -2) or Dox (PHPMA-Dox) were prepared. Zos was attached via a pH-sensitive hydrazone linker in order to allow release in the early stage of the endocytic process and maximize the cytosolic concentration of Zos in proximity of the P-gp transporter. Dox, in contrast, was conjugated to the PHPMA backbone via the lysosomally cleavable GFLG peptide linker.19, 28, 29 This was done to enhance release of Dox in close proximity of the nucleus, which was previously demonstrated to mitigate the effect of P-gp-mediated Dox efflux.19

INSERT SCHEME 1

The Zos- and Dox-modified PHPMA copolymers were prepared via a two-step post-polymerization modification strategy, starting from a side-chain reactive poly(pentafluorophenyl methacrylate) PPFMA precursor.30,31,32 Two different PPFMA polymers were chosen as the active-ester precursors and prepared by reversible addition-fragmentation chain transfer (RAFT) polymerization. PPFMA-1 was synthesized as previously reported by Gibson et al.,31 whereas PPFMA-2 was prepared using a fluorinated RAFT agent. The fluorinated label on the polymer backbone allowed the determination of the number average molecular weight (Mn) as well as the estimation of the Zos content of PPFMA-2 by 19F-NMR spectroscopy. Both PPFMA precursors were characterized by NMR spectroscopy and SEC and the detailed characterization is provided in Table S1. The PPFMA polymers were synthesized using monomer to chain transfer agent ratios of 200 for a period of 90 min, which resulted in 50%, respectively, 42%, monomer conversion. PPFMA-1 and PPFMA-2 had number average molecular weights (Mn) of 17210 and 27630 g/mol, respectively, as revealed by SEC. 19F-NMR analysis of PPFMA-2 revealed a Mn of 28220 g/mol, which is in good agreement with the SEC results. Dox was directly coupled to the PPFMA precursor by reacting part of the active ester moieties with the NH2-GFLG-modified Dox derivative shown in Chart 1. The Dox content of PHPMA-Dox was determined by 1H-NMR and UV-Vis analysis to be 2.5 mol%. To conjugate Zos, part of the PPFMA repeating units were first modified with 2-(pyridyldithio)-ethylamine (PDA) and 1-amino-2-propanol, followed by treatment with neutralized TCEP to generate side chain thiol functional groups and finally Michael addition of a maleimide-modified Zos derivative (Zos-Mal, Chart 1). By varying the amount of PDA used in the first post-polymerization step of PPFMA-1 and PPFMA-2, two different PHPMA-Zos conjugates were prepared, which contain 2.2 (PHPMA-Zos-1) and 4.3 (PHPMA-Zos-2) mol % Zos (1H-NMR spectroscopy), respectively. The dual functional PHPMA-Dox-Zos conjugate was obtained by first reacting PPFMA-2 with PDA and NH2-GFLG-Dox, followed by coupling of Zos-Mal and contains 2.9 and 0.2 mol % Dox and Zos, respectively (according to 1H-NMR spectroscopy). The characteristics of the different conjugates are summarized in Table 1 and Table S2. To conclude the discussion of the synthesis of the different polymers, it is worth noting that the structures of the polymers shown in Scheme 1 suggest complete conversion of all the pentafluorophenyl ester groups into the corresponding amides. It is, however, possible that the polymers contain a very small fraction (too small to be detected by 1H-NMR spectroscopy) of methacrylic acid repeat units that result from hydrolysis of the ester groups.33

INSERT CHART 1

INSERT TABLE 1

pH Triggered release of Zos-Ket from the PHPMA-Zos-1 conjugate

To verify that the incorporation of the hydrazone linker can facilitate pH triggered release of Zos, PHPMA-Zos-1 was placed in microdialysis cassettes both at pH 5.5 and 7.4 (physiological pH) and Zos release measured spectrophotometrically. The results of these experiments are shown in Figure 1 and confirm that release of Zos at pH 5.5 is significantly enhanced as compared to pH 7.4. It is important to note here that pH-induced cleavage of the hydrazone linker does not result in release of Zos but rather of Zos-Ket. At pH 5.5 release of Zos-Ket was found to level off at around 80 %. The incomplete hydrolysis of hydrazone-based polymer conjugates in model experiments has been previously reported.34 This behaviour was attributed to the reversible nature of the hydrazone bond and to the closed system used to investigate the release profile, which can result in the establishment of an equilibrium reaction between free drug and polymer-bound drug.

INSERT FIGURE 1

Cytotoxicity and P-gp inhibitory activity of Zos and Zos-Ket

To identify the concentration window that can be used for Zos and Zos-Ket combination therapy with Dox as well as to assess possible effects of the 4-acetylbenzoic acid modification on the P-gp inhibitory activity of Zos, the intrinsic cytotoxicity of Zos and Zos-Ket was first determined via the MTT assay using multidrug resistant A2780ADR and sensitive A2780 cells. Figure 2A presents the viability of both sensitive A2780 cells as well as multidrug resistant A2780ADR cells toward Zos and Zos-Ket at concentrations ranging from 10-3-10 M, The results in Figure 2A show that, while the viability of resistant cells was not significantly affected over the range of concentrations tested, the viability of the sensitive cells significantly decreased at 5 M for both Zos as well as Zos-Ket. This result is in agreement with the previously reported IC50 value of Zos in A2780 cells (11 M).23 The results in Figure 2A furthermore do not reveal any significant difference between Zos and Zos-Ket, indicating that chemical modification of the inhibitor has no influence on the cytotoxicity of this compound.

INSERT FIGURE 2

In order to investigate whether modification of Zos with 4-acetylbenzoic acid did affect the activity of this compound, the P-gp inhibitory activity of Zos and Zos-Ket was evaluated and compared in two different experiments. First, the ability of Zos and Zos-Ket to inhibit P-gp-mediated efflux of the model fluorescent dye DiOC2(3) from resistant A2780ADR cells was investigated by flow cytometry experiments. For these experiments, 20 M cyclosporine A (CsA), which is known to completely inhibit P-gp, was used as a positive control.35 Examples of flow cytometry experiments with Zos and Zos-Ket are presented in Supporting Information in Figure S29. Figure 2B presents the DiOC2(3) efflux inhibitory properties of Zos and Zos-Ket over a concentration range of 0.1-5 M relative to that of CsA. The results show that while 1 M Zos led to the complete inhibition of DiOC(3) efflux, 5 M Zos-Ket were necessary to achieve 78 % dye retention. On the other hand, more than 98 % DiOC2(3) was effluxed in the absence of an inhibitor. This indicates that chemical modification of Zos with 4-acetylbenzoic acid partially decreases its activity, however, at low micromolar concentrations the modified drug still retained the ability to inhibit 78 % DiOC2(3) efflux.

In a next series of experiments, the ability of Zos and Zos-Ket to increase Dox cytotoxicity in resistant cells was examined by the MTT assay. Sensitive and resistant cells were treated with Dox concentrations ranging from 0.1 nM to 20 M either alone or in combination with different concentrations of Zos and Zos-Ket. The results of these experiments are summarized in Figure 2C and Figure 2D. While resistant cells showed an expected high resistance to doxorubicin with an IC50 value of 1.441 M, the IC50 of the sensitive cells was 0.013 M. Figure 2C shows that co-administration of Dox and Zos-Ket to resistant cells resulted in a shift of the Dox cytotoxicity curve to lower concentrations in a Zos-Ket-dose dependent manner. Qualitatively similar results were obtained when resistant cells were treated with a combination of Dox and Zos (Figure S30A). Table 2 compares the Dox cytotoxicity toward both cell types at various Zos and Zos-Ket concentrations. The results in Table 2 indicate that at equal concentrations, Zos is more effective as compared to Zos-Ket in preventing efflux. For instance, when 1 M Zos and Zos-Ket were co-administered with Dox, the IC50 values towards the A2780ADR cells decreased to 0.048 and 0.068 M, respectively, and approached the value observed for sensitive cells (0.013 M). These IC50 values suggest that at a concentration of 1 M both inhibitors can sensitize resistant ovarian cancer cells to doxorubicin, but also indicate that the modification led to a slight decrease in activity, especially at low concentrations as evident from the higher IC50 values for Zos-Ket as compared to Zos at equal concentration. These results are in agreement with the efflux inhibitory experiments summarized in Figure 2B, which also indicate that Zos-Ket at identical concentration is less active as compared to Zos. Finally, as expected, the Dox IC50 values measured on the sensitive A2780 cells were not affected by co-administration of Zos or Zos-Ket (Figure 2D and Figure S30B).

INSERT TABLE 2

Cytotoxicity and P-gp inhibitory activity of PHPMA-Zos conjugates

In a next series of experiments, the cytotoxicity and P-gp inhibitory activity of PHPMA-Zos conjugates PHPMA-Zos-1 and PHPMA-Zos-2, which contain 2.2 and 4.3 mol % (1H-NMR) Zos, respectively, were investigated. The results of the MTT assay experiments that were done to assess the cytotoxicity are summarized in Figure 3A. The data in this Figure show that both polymers were nontoxic towards both cell lines within the concentration range investigated. In contrast, at a concentration of 10 M both Zos and Zos-Ket resulted in a significant reduced viability of A2780 cells (Figure 2A).

INSERT FIGURE 3

The P-gp inhibitory activity of the polymer-Zos conjugates was assessed using both the DiOC2(3) efflux assay as well as in cytotoxicity studies with co-administration of Dox. P-gp mediated efflux of DiOC2(3) from resistant A2780ADR cells after three hours incubation was investigated by flow cytometry. Figure S29C and D shows examples of flow cytometry results, which were obtained with PHPMA-Zos-1 and PHPMA-Zos-2. From these flow cytometry experiments, the P-gp inhibitory activity of the polymer conjugates was determined and expressed as a percentage relative to the CsA positive control. Figure 3B, which summarizes the results obtained from duplicate experiments, clearly shows that incubation of the cells with 5 M of polymer-bound drug led to complete inhibition of DiOC2(3) efflux. In contrast, it was shown in the previous section that the same concentration of free Zos-Ket resulted only in 78 % dye retention. Moreover, Figure 3B also shows  that the activity of PHPMA-Zos-2 is slightly lower than that of PHPMA-Zos-1 at 0.1 and 1 M polymer-bound Zos-Ket. The enhanced P-gp inhibitory activity of PHPMA-Zos-1 as compared to free Zos-Ket at equal Zos-concentrations may be interpreted in terms of the enhanced internalization of the polymer-bound drug. In a next series of experiments A2780ADR cells were exposed to the polymer-Zos conjugates at three concentrations and Dox IC50 values were determined using the MTT assay. The results of these experiments are summarized in Figure 3C and D and in Table 2. Similar to what has been observed for free Zos-Ket, the IC50 values of the resistant cells reached a minimum when 1 M of polymer-bound Zos-Ket was co-administered with Dox. However, it is worth mentioning that at lower concentrations, the IC50 values of the polymer-bound Zos-Ket were significantly lower than those previously found for free Zos-Ket and were almost in the same range as those found for Zos. For instance, 0.1 M of Zos-Ket delivered as PHPMA-Zos-1 and PHPMA-Zos-2 decreased the Dox IC50 to 0.053 and 0.069 M, respectively, whereas these values were 0.051 M for free Zos and 0.341 M for Zos-Ket. Moreover, similar to what was observed when free drugs were used, the co-administration of both polymers and Dox did not show any effect on the sensitive A2780 cells (Figure S30C and D).

Efflux inhibition and cytotoxicity of PHPMA-Dox conjugates

In a final set of experiments, the efflux inhibitory properties and cytotoxicity of the different polymer-bound Dox conjugates were evaluated. To this end, first the intrinsic cytotoxicity of PHPMA-Dox was determined and the accumulation of Dox in the A2780ADR cells when administered using the different polymer conjugates compared, before assessing the cytostatic activity of PHPMA-Dox-Zos conjugate. To determine the cytotoxicity of the PHPMA-Dox conjugate, cells were incubated with a range of PHPMA-Dox concentrations and their viability was determined by MTT assay. Figure S31 shows cytotoxicity curves of PHPMA-Dox as well as of free Dox in both sensitive and resistant cells and the correspondent IC50 values are listed in Table S3. While the IC50 of free Dox in resistant cells was 1.441 M, the IC50 of the sensitive cells was 0.013 M. The concentration of PHPMA-Dox necessary to lower the cell viability to values around 50 % was much higher for both cell lines (around 20 M for sensitive and 100 M for resistant cells). The IC50 values for free Dox indicate a resistance ratio of 111, whereas a value around 5 is estimated when doxorubicin is delivered as PHPMA-Dox. These results are in agreement with previously published data19 and suggest that, while the IC50 values of the polymer conjugate increases as compared to the free Dox, the resistance ratio significantly decreases.

Next, Dox accumulation in A2780ADR cells when administered as free drug or delivered as PHPMA-Dox (2.4 mol % of Dox) or PHPMA-Dox-Zos (2.9 mol % of Dox and 0.2 mol % of Zos) conjugates was investigated by flow cytometry experiments. Cells were incubated with 10 M Dox or polymer-bound Dox, either alone or in combination with 20 M of the positive control CsA for 4 h. In the case of PHPMA-Dox-Zos, the calculated concentration of polymer-bound Zos-Ket is 0.7 M. CsA was used to determine the maximum Dox accumulation in each experiment, allowing for the direct comparison of the results while neglecting eventual different cellular internalization rates of the tested compounds. Flow cytometry data from these experiments are shown in Figure S32 and the Dox retention, expressed as a percentage relative to the CsA positive control cells, are presented in Figure 4A. The results in Figure 4A show that Dox retention was lowest when cells were treated with free Dox. At a Dox concentration of 10 M treating A2780 ADR cells with PHPMA-Dox or PHPMA-Dox-Zos resulted in a 8 and 10 fold higher accumulation of Dox, respectively, as compared to the use of free Dox. These results confirm that (i) the administration of polymer-bound Dox decreases drug efflux from resistant cells and (ii) dual delivery of Dox and Zos using a single polymer conjugate even further reduces drug efflux by inhibiting the P-gp transporter.

INSERT FIGURE 4

While the experiments discussed above demonstrate that co-delivery of Dox and Zos is an efficient strategy to reduce P-gp mediated efflux, it should be noted that the time course of these experiments (4 hours) may not be sufficient for all Dox and Zos to be released. Therefore, also the cytostatic activity of the PHPMA-Dox conjugate, both alone, as well as in combination with Zos, Zos-Ket and PHPMA-Zos-1 was determined and compared with that of the dual functional PHPMA-Dox-Zos conjugate using MTT assay after an incubation time of 72 h. Due to the fact that both drugs are attached to the same polymer carrier, it was not possible to determine the cytotoxicity curve and therefore the IC50 value for the PHPMA-Dox-Zos conjugate. Cell incubation with increasing amount of polymer-bound Dox, would also cause cell exposure to increasing concentrations of the polymer-bound P-gp inhibitor. Hence, for this particular experiment, the cell viability was determined at a selected Dox concentration. Based on the mol % of functionalization of the polymer carrier with the two drugs, the concentration of Zos was calculated. The selected Dox concentration in each experiment was 20 M, which is close to the IC50 of PHPMA-Dox in sensitive cells and does not significantly affect the viability of the resistant cells. Since the ratio between the concentration of Dox and the concentration of the inhibitor was 14.5 in the PHPMA-Dox-Zos conjugate, in all the experiments the concentration of polymer-bound inhibitor was 1.4 M. Figure 4B illustrates that the treatment of sensitive cells with the PHPMA-Dox conjugate, either alone or in combination with 2 M of the inhibitors (Zos, Zos-Ket and PHPMA-Zos-1), led to an approximate cell viability of 50 % (Experiments using PHPMA-Dox in combination with 1 M inhibitors led to comparable results, data not shown). On the other hand, while the viability of the resistant cells in the presence of PHPMA-Dox was 83 %, the co-administration of the this conjugate with the inhibitors led to cell viabilities comparable to that of sensitive cells. Finally, treatment of the sensitive cells with the dual functional PHPMA-Dox-Zos conjugate also resulted in a cell viability of ~ 50% similar to what was obtained for the co-administration of PHPMA-Dox with Zos, Zos-Ket or PHPMA-Zos-1. While in vitro co-administration of PHPMA-Dox with a polymer-bound P-gp inhibitor is equally effective in mitigating the effect of drug efflux on the viability of A2780ADR cells as using the dual functional PHPMA-Dox-Zos conjugate, the use of a combination polymer therapeutic offers a number of advantages in vivo. Most important, the use of a single polymer carrier allows to overcome challenges that are due to differences in the pharmacokinetics of the two low molar mass drugs, since the pharmacokinetics of the conjugate are dictated and can be controlled by engineering the polymer conjugate. Another benefit of the use of a dual functional conjugate such as PHPMA-Dox-Zos is that it allows to administer and intracellularly deliver the chemotherapeutic and the P-gp inhibitor at a precisely defined and controlled ratio.36

CONCLUSIONS

This contribution has reported the preparation and properties of a dual-functional PHPMA conjugate that allows spatially controlled release of the anticancer drug Dox and the third generation P-gp inhibitor Zos by using two orthogonally cleavable linkers. First, the feasibility of PHPMA conjugates bearing a Zos derivative via a hydrazone linker as an effective polymeric system to overcome Dox efflux in resistant ovarian cancer cells was investigated. Two different PHPMA-Zos conjugates containing 2.2 (PHPMA-Zos-1) and 4.3 (PHPMA-Zos-2) mol % Zos-Ket, respectively, were prepared. Both conjugates showed a reduced intrinsic cytotoxicity in sensitive cells compared to free inhibitors. More importantly, it was found that polymer-mediated delivery of Zos-Ket enhanced its activity and therefore increased Dox cytotoxicity in resistant ovarian carcinoma cells. After that, the in vitro activity of a PHPMA conjugate containing Dox alone (PHPMA-Dox) was compared with that of a dual functional conjugate presenting both Zos and Dox (PHPMA-Dox-Zos). First, the ability of the control PHPMA-Dox conjugate to partially overcome MDR in resistant A2780ADR cells was confirmed. Finally, it was demonstrated that the presence of the two drugs attached to the polymer backbone via orthogonally cleavable linkers enhanced P-gp inhibition as compared to the PHPMA-Dox conjugate and led to a doxorubicin cytotoxicity comparable to that of the sensitive A2780 cells. This result is of interest for in vivo applications, in which the use of a single polymer carrier for the delivery of multiple drugs allows simultaneous intracellular accumulation of the two drugs in a predetermined therapeutic ratio.

ACKNOWLEDGMENTS

This research has been financially supported by Swiss National Science Foundation (SNSF).

Supporting Information. Additional synthetic procedures, 1H-, 13C- and 19F-NMR spectra, UV-Vis spectra and flow cytometry data. This material is available free of charge via the Internet at http://pubs.acs.org

REFERENCES

1.	Eckford, P. D.; Sharom, F. J., ABC efflux pump-based resistance to chemotherapy drugs. Chem. Rev. 2009, 109 (7), 2989-3011.

2.	Longley, D. B.; Johnston, P. G., Molecular mechanisms of drug resistance. J. Pathol. 2005, 205 (2), 275-292.

3.	Szakacs, G.; Paterson, J. K.; Ludwig, J. A.; Booth-Genthe, C.; Gottesman, M. M., Targeting multidrug resistance in cancer. Nat. Rev. Drug Discovery 2006, 5 (3), 219-234.

4.	Fletcher, J. I.; Haber, M.; Henderson, M. J.; Norris, M. D., ABC transporters in cancer: more than just drug efflux pumps. Nat. Rev. Cancer 2010, 10 (2), 147-156.

5.	Abolhoda, A.; Wilson, A. E.; Ross, H.; Danenberg, P. V.; Burt, M.; Scotto, K. W., Rapid activation of MDR1 gene expression in human metastatic sarcoma after in vivo exposure to doxorubicin. Clin. Cancer Res. 1999, 5 (11), 3352-3356.

6.	Trock, B. J.; Leonessa, F.; Clarke, R., Multidrug resistance in breast cancer: a meta-analysis of MDR1/gp170 expression and its possible functional significance. J. Natl. Cancer Inst. 1997, 89 (13), 917-31.

7.	Arao, S.; Suwa, H.; Mandai, M.; Tashiro, H.; Miyazaki, K.; Okamura, H.; Nomura, H.; Hiai, H.; Fukumoto, M., Expression of multidrug resistance gene and localization of P-glycoprotein in human primary ovarian cancer. Cancer Res. 1994, 54 (5), 1355-9.

8.	Pallis, M.; Russell, N., Strategies for overcoming p-glycoprotein-mediated drug resistance in acute myeloblastic leukaemia. Leukemia 2004, 18 (12), 1927-30.

9.	Ambudkar, S. V.; Kimchi-Sarfaty, C.; Sauna, Z. E.; Gottesman, M. M., P-glycoprotein: from genomics to mechanism. Oncogene 2003, 22 (47), 7468-85.

10.	Ozben, T., Mechanisms and strategies to overcome multiple drug resistance in cancer. Febs Lett. 2006, 580 (12), 2903-2909.

11.	Callaghan, R.; Luk, F.; Bebawy, M., Inhibition of the multidrug resistance P-glycoprotein: time for a change of strategy? Drug. Metab. Dispos. 2014, 42 (4), 623-31.

12.	Montesinos, R. N.; Beduneau, A.; Pellequer, Y.; Lamprecht, A., Delivery of P-glycoprotein substrates using chemosensitizers and nanotechnology for selective and efficient therapeutic outcomes. J. Controlled Release 2012, 161 (1), 50-61.

13.	Ajaj, K. A.; Kratz, F., Development of dual-acting prodrugs for circumventing multidrug resistance. Bioorg. Med. Chem. Lett. 2009, 19 (3), 995-1000.

14.	Parhi, P.; Mohanty, C.; Sahoo, S. K., Nanotechnology-based combinational drug delivery: an emerging approach for cancer therapy. Drug Discovery Today 2012, 17 (17-18), 1044-1052.

15.	Duncan, R., Polymer conjugates as anticancer nanomedicines. Nat. Rev. Cancer 2006, 6 (9), 688-701.

16.	Danhier, F.; Feron, O.; Preat, V., To exploit the tumor microenvironment: Passive and active tumor targeting of nanocarriers for anti-cancer drug delivery. J. Controlled Release 2010, 148 (2), 135-46.

17.	Gruenberg, J., The endocytic pathway: a mosaic of domains. Nat. Rev. Mol. Cell Biol. 2001, 2 (10), 721-30.

18.	Davis, M. E.; Chen, Z. G.; Shin, D. M., Nanoparticle therapeutics: an emerging treatment modality for cancer. Nat. Rev. Drug Discovery 2008, 7 (9), 771-82.

19.	Minko, T.; Kopeckova, P.; Pozharov, V.; Kopecek, J., HPMA copolymer bound adriamycin overcomes MDR1 gene encoded resistance in a human ovarian carcinoma cell line. J. Controlled Release 1998, 54 (2), 223-33.

20.	Minko, T.; Kopeckova, P.; Kopecek, J., Chronic exposure to HPMA copolymer-bound adriamycin does not induce multidrug resistance in a human ovarian carcinoma cell line. J. Controlled Release 1999, 59 (2), 133-48.

21.	Binichathlan, Z.; Hamdy, D. A.; Brocks, D. R.; Lavasanifar, A., Development of a polymeric micellar formulation for valspodar and assessment of its pharmacokinetics in rat. Eur. J. Pharm. Biopharm. 2010, 75 (2), 90-95.

22.	Subr, V.; Sivak, L.; Koziolova, E.; Braunova, A.; Pechar, M.; Strohalm, J.; Kabesova, M.; Rihova, B.; Ulbrich, K.; Kovar, M., Synthesis of Poly[N-(2-hydroxypropyl)methacrylamide] Conjugates of Inhibitors of the ABC Transporter That Overcome Multidrug Resistance in Doxorubicin-Resistant P388 Cells in Vitro. Biomacromolecules 2014, 15 (8), 3030-3043.

23.	Dantzig, A. H.; Shepard, R. L.; Cao, J.; Law, K. L.; Ehlhardt, W. J.; Baughman, T. M.; Bumol, T. F.; Starling, J. J., Reversal of P-glycoprotein-mediated multidrug resistance by a potent cyclopropyldibenzosuberane modulator, LY335979. Cancer Res. 1996, 56 (18), 4171-4179.

24.	Tong, R.; Tang, L.; Ma, L.; Tu, C. L.; Baumgartner, R.; Cheng, J. J., Smart chemistry in polymeric nanomedicine. Chem. Soc. Rev. 2014, 43 (20), 6982-7012.

25.	Abu Ajaj, K.; Graeser, R.; Kratz, F., Zosuquidar and an albumin-binding prodrug of zosuquidar reverse multidrug resistance in breast cancer cells of doxorubicin and an albumin-binding prodrug of doxorubicin. Breast Cancer Res. Treat. 2012, 134 (1), 117-129.

26.	Eberhardt, M.; Mruk, R.; Zentel, R.; Theato, P., Synthesis of pentafluorophenyl(meth)acrylate polymers: New precursor polymers for the synthesis of multifunctional materials. Eur. Polym. J. 2005, 41 (7), 1569-1575.

27.	Apostolovic, B.; Klok, H. A., pH-sensitivity of the E3/K3 heterodimeric coiled coil. Biomacromolecules 2008, 9 (11), 3173-80.

28.	Zhong, Y. J.; Shao, L. H.; Li, Y., Cathepsin B-cleavable doxorubicin prodrugs for targeted cancer therapy (Review). Int. J. Oncol. 2013, 42 (2), 373-383.

29.	Rejmanova, P.; Kopecek, J.; Pohl, J.; Baudys, M.; Kostka, V., Polymers Containing Enzymatically Degradable Bonds .8. Degradation of Oligopeptide Sequences in N-(2-Hydroxypropyl)Methacrylamide Co-Polymers by Bovine Spleen Cathepsin-B. Makromolekulare Chemie-Macromolecular Chemistry and Physics 1983, 184 (10), 2009-2020.

30.	Barz, M.; Tarantola, M.; Fischer, K.; Schmidt, M.; Luxenhofer, R.; Janshoff, A.; Theato, P.; Zentel, R., From Defined Reactive Diblock Copolymers to Functional HPMA-Based Self-Assembled Nanoaggregates. Biomacromolecules 2008, 9 (11), 3114-3118.

31.	Gibson, M. I.; Frohlich, E.; Klok, H. A., Postpolymerization Modification of Poly(Pentafluorophenyl methacrylate): Synthesis of a Diverse Water-Soluble Polymer Library. J. Polym. Sci., Part A: Polym. Chem. 2009, 47 (17), 4332-4345.

32. Nuhn, L.; Barz, M.; Zentel, R., New Perspectives of HPMA-based Copolymers Derived by Post-Polymerization Modification, Macromol. Biosci. 2014, 14, 607–618.

33. Mohr, N.; Barz, M.; Forst, R.; Zentel, R., A Deeper Insight into the Postpolymerization Modification of Polypenta Fluorophenyl Methacrylates to Poly(N-(2-Hydroxypropyl) Methacrylamide), Macromol. Rapid Commun. 2014, 35, 1522−1527.

34.	Christie, R. J.; Anderson, D. J.; Grainger, D. W., Comparison of Hydrazone Heterobifunctional Cross-Linking Agents for Reversible Conjugation of Thiol-Containing Chemistry. Bioconjugate Chem. 2010, 21 (10), 1779-1787.

35.	Ansbro, M. R.; Shukla, S.; Ambudkar, S. V.; Yuspa, S. H.; Li, L. W., Screening Compounds with a Novel High-Throughput ABCB1-Mediated Efflux Assay Identifies Drugs with Known Therapeutic Targets at Risk for Multidrug Resistance Interference. Plos One 2013, 8 (4).

36.	Xu, X. Y.; Ho, W.; Zhang, X. Q.; Bertrand, N.; Farokhzad, O., Cancer nanomedicine: from targeted delivery to combination therapy. Trends Mol. Med. 2015, 21 (4), 223-232.

Table 1. Composition of the PHPMA conjugates investigated in this study.

| Sample | Zos content (mol %) |  | Dox content (mol %) |  |
| --- | --- | --- | --- | --- |
|  | 1H-NMRa | 19F-NMRb | 1H-NMRc | UVd |
| PHPMA-Zos-1 | 2.2 | - | - | - |
| PHPMA-Zos-2 | 4.3 | 4.6 | - | - |
| PHPMA-Dox | - | - | 2.4 | 2.5 |
| PHPMA-Dox-Zos | 0.2 | 0.4 | 2.9 | 2.9 |

a Determined by comparing the integrals of Zos signals with those of the polymer backbone and with the CH proton of the hydroxypropyl polymer side chains.

b Determined by comparing the integrals of fluorine signals of Zos with those of the polymer end group and taking into account the degree of polymerization (DP).

c Determined by comparing the integrals of the Dox signals with those of the polymer backbone and with the CH proton of the hydroxypropyl polymer side chains.

d Calculated from the absorbance peak at  = 490 nm in DMSO ( = 12049.6 cm-1 M-1).

Table 2. Cytotoxicity of doxorubicin alone and in combination with Zos, Zos-Ket and the PHPMA-Zos conjugates PHPMA-Zos-1 and PHPMA-Zos-2 in sensitive A2780 and resistant A2780ADR cells as determined by the MTT assay.

| Compound | [P-gp inhibitor] (M) | Dox IC50 (M) |  |
| --- | --- | --- | --- |
|  |  | A2780 | A2780ADR |
| Dox | - | 0.013 ± 0.003 | 1.441 ± 0.361 |
| Zos | 0.01 | 0.022 ± 0.006 | 0.198 ± 0.078 |
|  | 0.1 | 0.032 ± 0.002 | 0.051 ± 0.014 |
|  | 1 | 0.017 ± 0.002 | 0.048 ± 0.006 |
| Zos-Ket | 0.01 | 0.020 ± 0.006 | 1.474 ± 0.352 |
|  | 0.1 | 0.010 ± 0.004 | 0.341 ± 0.071 |
|  | 1 | 0.011 ± 0.004 | 0.068 ± 0.006 |
| PHPMA-Zos-1 | 0.01 | 0.008 ± 0.001 | 0.174 ± 0.010 |
|  | 0.1 | 0.006 ± 0.004 | 0.053 ± 0.017 |
|  | 1 | 0.007 ± 0.003 | 0.018 ± 0.007 |
| PHPMA-Zos-2 | 0.01 | 0.012 ± 0.002 | 1.098 ± 0.194 |
|  | 0.1 | 0.011 ± 0.007 | 0.069 ± 0.025 |
|  | 1 | 0.013 ± 0.003 | 0.053 ± 0.015 |

Chart 1. Chemical structures of Zos, Zos-Ket, Zos-Mal and NH2-GFLG-Dox.

Scheme 1. Synthesis of the PHPMA-drug conjugates investigated in this study.

Figure 1. Cumulative release of Zos-Ket from PHPMA-Zos-1 in phosphate citrate buffer at pH 7.4 (○) and 5.5 (●) at 37 °C as a function of time over 40 hours.

Figure 2. (A) Intrinsic cytotoxicity of Zos and Zos-Ket toward sensitive A2780 and resistant A2780ADR cells as determined by the MTT assay after 72 h. Data are significantly different by Student’s t test: *** (P < 0.001) and ** (P < 0.01). (B) Inhibition of DiOC2(3) efflux from A2780ADR cells. Cells were incubated with varying concentrations of Zos, Zos-Ket as well as with 20 M cyclosporine A (CsA) at 37°C for 3 hours. After 20 minutes exposure to DiOC2(3), cells were washed and incubated at 37°C with and without the P-gp inhibitors for an additional 90 minutes and finally analysed by flow cytometry. The relative fluorescence represents the ratio between the geometric mean fluorescence of each sample and the positive control CsA. (C) Dox cytotoxicity alone and in combination with increasing concentrations of Zos-Ket in A2780ADR and (D) A2780 cells. MTT results were read after 72 h incubation and are reported with respect to the percentage of untreated cells.

Figure 3. (A) Intrinsic cytotoxicity of PHPMA-Zos-1 and PHPMA-Zos 2 toward sensitive A2780 and resistant A2780ADR cells as determined by the MTT assay after 72 h. (B) Inhibition of DiOC2(3) efflux from A2780ADR cells. Cells were incubated with varying concentrations of PHPMA-Zos-1 and PHPMA-Zos 2 as well as with 20 M cyclosporine A (CsA) at 37°C for 3 hours. After 20 minutes exposure to DiOC2(3), cells were washed and incubated at 37°C with and without the P-gp inhibitors for an additional 90 minutes and finally analysed by flow cytometry. The relative fluorescence represents the ratio between the geometric mean fluorescence of each sample and the positive control CsA. (C) Dox cytotoxicity alone and in combination with increasing concentrations of PHPMA-Zos-1 and (D) PHPMA-Zos-2 in A2780ADR cells. MTT results were read after 72 h incubation and are reported with respect to the percentage of untreated cells. The concentrations of P-gp inhibitor are always expressed as polymer-bound drug.

Figure 4. (A) Comparison between Dox efflux from A2780ADR cells when administered as free drug or delivered as PHPMA-Dox or PHPMA-Dox-Zos conjugate. Cells were incubated with 10 M Dox and polymer-bound Dox either alone or in combination with 20 M of CsA for 4 hours and subsequently washed with fresh medium twice and analysed by flow cytometry. The relative fluorescence represents the ratio between the geometric mean fluorescence of each sample and the samples containing also the positive control CsA. (B) Sensitization of A2780ADR cells by using the PHPMA-Dox-Zos conjugate. Cells, either sensitive A2780 (shaded bars) or resistant A2780ADR (gray bars) were incubated with 20 M of free Dox and PHPMA-bound Dox either alone or in combination with 2 M of the P-gp inhibitors Zos, Zos-Ket and PHPMA-Zos-1 and with the PHPMA-Dox-Zos conjugate (20 M of Dox and 1.4 M of Zos). MTT results were read after 72 h incubation and are reported with respect to the percentage of untreated cells. In both assays data are significantly different by Student’s t test: *** (P < 0.001) and * (P < 0.05).

For Table of Contents Use Only

Reversion of P-gp-mediated Drug Resistance in Ovarian Carcinoma Cells with PHPMA-Zosuquidar Conjugates

Claudia Battistella and Harm-Anton Klok*